C.20733

C.20733

West Yorkshire Fire & Rescue Service

Bradford Fire Station

V1

NBS SPECIFICATION

Tender

18-03-2025

Contents

C20 Demolition	1

C90 Alterations	3

F10 Brick/ block walling	4

F30 Accessories/ sundry items for brick/ block/ stone walling	7

G20 Carpentry/ timber-framing/ first fixing	10

K10 Gypsum board dry linings/ partitions/ ceilings	12

K40 Demountable suspended ceilings	20

L20 Doors/ shutters/ hatches	25

M10 Cement based levelling/ wearing screeds	27

M20 Plastered/ rendered/ roughcast coatings	30

M40 Stone/ concrete/ quarry/ ceramic tiling/ mosaic	34

M50 Rubber/ plastics/ cork/ lino/ carpet tiling/ sheeting	37

M60 Painting/ clear finishing	40

N13 Sanitary appliances and fittings	45

N15 Internal fire and safety signage systems	50

P12 Fire-stopping systems	52

P21 Door/ window ironmongery	55

P31 Holes, chases, covers and supports for services	59

Z10 Purpose-made joinery	61

Z11 Purpose-made metalwork	62

Z12 Preservative/ flame-retardant treatment	64

Z20 Fixings and adhesives	66

Z21 Mortars	68

Z22 Sealants	70

C20
Demolition

To be read with preliminaries/ general conditions.

30 	Services disconnection arranged by contractor

- General: Arrange with the appropriate authorities and responsible private organizations for disconnection of services, and removal of fittings and equipment owned by those authorities and organizations where agreed, prior to starting deconstruction or demolition

50 	Workmanship

- Standard: Demolish structures in accordance with BS 6187.

- Operatives

  - Appropriately skilled and experienced for the type of work.

  - Holding, or in training to obtain, relevant Construction Skills certification of competence.

- Site staff responsible for supervision and control of work: Experienced in the assessment of risks involved and methods of deconstruction and demolition to be used. Hold appropriate qualification or training certificates for their role.

55 	Site hazards

- Precautions: Prevent fire or explosion caused by gas and vapour from tanks, pipes, etc. Identify potential sources and assess risk prior to commencement of works on site.

- Dust: Minimize airborne dust by periodically spraying deconstruction and demolition works with an appropriate wetting agent. Keep public roadways and footpaths clear of mud and debris

  - Dust suppression and reduction: Submit method statement for control, containment and clean-up regimes. Submit documentation outlining additional lead dust controls

- Site operatives and general public: Protect from health hazards including those associated with vibration, dangerous fumes and dust arising during the course of the works.

71 	Dangerous openings

- General: Provide guarding at all times, including outside of working hours. Illuminate during hours of darkness.

- Access: Prevent access by unauthorized persons.

76 	Asbestos-containing materials – unknown occurrences

- Discovery: Stop work, and give immediate notice of suspected asbestos-containing materials when they are discovered during deconstruction and demolition work. Avoid disturbing such materials.

- Removal: Submit statutory risk assessments and details of proposed methods for safe removal.

78 	Unforeseen hazards

- Discovery: Give notice immediately when hazards, such as unrecorded voids, tanks, chemicals, are discovered during deconstruction or demolition.

- Removal: Submit details of proposed methods for filling, removal, etc.

85 	Site condition at completion

- Debris: Clear away and leave the site in a clean, tidy, safe and secure condition.

- Other requirements: Identify removed contaminants in the health and safety file.

95 	Recycled materials

- Materials arising from deconstruction and demolition work:: Can be recycled or reused elsewhere in the project, subject to compliance with the appropriate specification and in accordance with the site waste management plan.

- Verification

  - Evidence of compliance: Submit full details and supporting documentation.

  - Timing: Allow adequate time in programme for verification of compliance.

Ω End of Section

C90
Alterations

To be read with preliminaries/ general conditions. - Not Used

General

110 	Alteration works

- Items: Refer to Schedule of Work

- Locations: Refer to contract drawings

130 	Recycled content

- Materials arising from alterations: May be recycled or reused elsewhere in the project, subject to compliance with the appropriate specification and in accordance with any site waste management plan.

140 	Removal

- Scope: Refer to contract drawings

Ω End of Section

F10
Brick/ block walling

Clauses

36 	Concrete common blockwork

- Description: IN PARTITIONS

- Blocks: To BS EN 771-3.

  - Manufacturer: Thomas Armstrong (Concrete Blocks) Ltd or similar, equal and approved.

  - Configuration: Group 1

  - Compressive strength: 10.4 N/mm²

  - Category: I

  - Freeze/ thaw resistance: Frost resistant

  - Recycled content: Contractor's choice

  - Work sizes (length x width x height): 440 x 140 x 215 mm or 440 x 100 x 215 mm to suit existing opening thickness.

    - Tolerance category: D1

  - Additional requirements: Reaction to fire class: A1

- Mortar: As section Z21.

  - Standard: To BS EN 998-2

  - Mix: 1:1:6 cement:lime:sand

- Bond: Half lap stretcher or to match existing.

36 	Aggregate concrete blocks Type A

- Contact details

  - Address: Whinfield Road
Rowlands Gill
Newcastle-upon-Tyne
Tyneside
United Kingdom
NE39 1EH

  - Telephone: +44 (0)1207 544214

  - Web: https://www.thomasarmstrongconcreteblocks.co.uk

  - Email: blocks@thomasarmstrong.co.uk

- Blocks: To BS EN 771-3.

  - Manufacturer: Thomas Armstrong (Concrete Blocks) Ltd

  - Product reference: Dense Paint-Grade Concrete Block (140 mm)

  - Standard: To BS EN 771-3.

  - Block description: Close textured or paint grade block.

  - Configuration: To BS EN 1996-1-1, Solid group 1.

  - Compressive strength

    - Mean value: 10.4 N/mm².

    - Category: II.

  - Freeze/ thaw resistance: Freeze thaw resistant.

  - Thermal conductivity: 1.17 W/mK (inner leaf). 1.26 W/mK (outer leaf).

  - Recycled content: 20%.

  - Work sizes (length x width x height): 440 x 140 x 215 mm or 440 x 100 x 215 mm to suit existing opening thickness.

  - Tolerance category: D1.

  - Density

    - Gross dry density: 1850-2100 kg/m³.

  - Reaction to fire: To BS EN 13501-1, Class A1.

  - Water vapour permeability: 5/15 µ.

  - Moisture movement: 0.6 mm/m.

  - R-Value: 0.12 m²k/W.

  - Weight: 266 kg/m²: walled weight. 25.2 kg: block weight.

  - Sound reduction: 51 dB (Rw).

51 	Basic workmanship

- Bond where not specified: Half lap stretcher.

- Mortar joints: Fill all vertical joints. Lay bricks, solid and cellular blocks on a full bed.

- AAC block thin mortar adhesive and gypsum block adhesive joints: Fill vertical joints. Lay blocks on a full bed.

- Clay block joints

  - Thin layer mortar: Lay blocks on a full bed.

  - Interlocking perpends: Butted.

- Quoins and advance work: Rack back.

- Locations for equal levelling of cavity wall leaves

  - Every course containing vertical twist type ties or other rigid ties.

  - Every third tie course for double triangle/ butterfly ties.

  - Courses in which lintels are to be bedded.

- Lift height (maximum) for walling using cement gauged or hydraulic lime mortar: 1.2 m above any other part of work at any time.

- Daily lift height (maximum) for walling using cement gauged or hydraulic lime mortar: 1.5 m for any one leaf.

- Lift height (maximum) for walling using thin layer mortar: 1.3 m above any other part of work at any time.

55 	Facework

- Commencement of facework: Not less than 150 mm below finished level of adjoining ground or external works level.

- Brick/ block selection: Do not use units with damaged faces or arrises.

- Cut masonry units: Where cut faces or edges are exposed cut with table masonry saw.

- Coursing brickwork and concrete blockwork: Evenly spaced using gauge rods. To produce satisfactory junctions and joints with built-in elements and components.

60 	Alterations/ Extensions

- Coursing: Line up with existing work.

- Block bonding new walls to existing: Unless agreed otherwise cut pocket requirements as follows:

  - Width: Full thickness of new wall.

  - Depth (minimum): 100 mm.

  - Vertical spacing: As follows:

  - Brick to brick: 4 courses high at 8 course centres.

  - Block to block: Every other course.

  - Pocket joints: Fully filled with mortar.

- New and existing facework in the same plane: Bonded together at every course to achieve continuity of bond and coursing.

- Support of existing work: Fully consolidate joint above inserted lintel or masonry with semidry mortar to support existing structure.

66 	Fire stopping

- Avoidance of fire and smoke penetration: Fit tightly between cavity barriers and masonry. Leave no gaps.

Ω End of Section

F30
Accessories/ sundry items for brick/ block/ stone walling

To be read with preliminaries/ general conditions.

6 	Cleanliness

- Cavity base and faces, ties, insulation and exposed dpcs: Free from mortar and debris.

18 	Cavity closers

- Manufacturer: Contractor's choice

  - Product reference: Contractor's choice

- Accessories: To include integral insulation

18 	Plastics cavity closers Type A

- Manufacturer: Kingspan Insulation

  - Contact details

    - Address: Kingspan Insulation Ltd
Pembridge
Leominster
Herefordshire
United Kingdom
HR6 9LA

    - Telephone: +44 (0)1544 388601

    - Web: https://www.kingspan.com/gb/en-gb

    - Email: info@kingspaninsulation.co.uk

  - Product reference: Kingspan Thermabate Cavity Closer (Kingspan Thermabate Cavity Closer - Single Flange: 100 mm)

- Third-party certification: British Board of Agrément (BBA) Certification.

- Accessories: As required.

- To fit cavity width: 100 mm.

- Length (effective): 3000 mm.

- MassDensity: 32 g/cm³.

- ThermalConductivity: 0.034 W/m∙K.

26 	Head restraint slip ties Type A

- Description: For 1F Blockwork Bedroom Partitions

- Type: Slip ties – wall head restraint

- Manufacturer: Vista Engineering Ltd

  - Contact details

    - Address: Carr Brook Works
Elnor Lane
Whaley Bridge
High Peak
Derbyshire
SK23 7JN

    - Telephone: +44 (0)1663 736700

    - Web: https://www.vistaeng.co.uk

    - Email: sales@vistaeng.co.uk

  - Product reference: Head Restraints (VHR head restraints)

- Material: Grade 304 stainless steel.

- Length: Manufacturer's standard.

- End types: Asymmetrical flat plates for mortar bedding, holed.

- Design embedment length (minimum): Manufacturer's standard.

- Additional requirements

  - Mortar joint thickness (minimum): Manufacturer's standard.

  - Shear load capacity: Manufacturer's standard.

- Type: VHR Head restraint, 100 or 140 mm walls.

- Fixing: Manufacturer's standard.

39 	Wall starters and connectors Type A

- Manufacturer: Wincro Metal Industries Ltd

  - Contact details

    - Address: Wincobank Works
3 Fife Street
Sheffield
South Yorkshire
S9 1NJ

    - Telephone: +44 (0)114 242 2171

    - Web: https://www.wincro.com

    - Email: spec@wincro.com

  - Product reference: Wall Extension System

- Material: Stainless steel, grade 1.4301 (304).

- Tie type: Channel, screws and ties.

- Sizes

  - Channel length: 3.0 m.

- Accessories: WBPS.

- Pack includes: 2 x 1.2 m interlocking stainless steel channel lengths; 10 x twist, lock & slide stainless steel wall ties (WTP3C36 or WTS3C36); 5 x stainless steel coach screws, washers & plugs.

- Maximum wind loading: 4.5 kN over 2400 mm.

- Ties: As required

39 	Wall starters and connectors Type B

- Manufacturer: Wincro Metal Industries Ltd

  - Contact details

    - Address: Wincobank Works
3 Fife Street
Sheffield
South Yorkshire
S9 1NJ

    - Telephone: +44 (0)114 242 2171

    - Web: https://www.wincro.com

    - Email: spec@wincro.com

  - Product reference: Wall Starter Kits

- Material: Stainless steel, grade 1.4301 (304).

79 	Head of non-loadbearing walls

- Restraints: As Clause 26

  - Fixing: Secure to soffit.

- Joint filler: Firestopping; Contractors proposal.

  - Placement: Full, no gaps

Ω End of Section

G20
Carpentry/ timber-framing/ first fixing

Clauses

2 	Timber procurement

- Timber (including timber for wood-based products): Obtained from well-managed forests/ plantations in accordance with:

  - The laws governing forest management in the producer country or countries.

  - International agreements such as the Convention on International Trade in Endangered Species of Wild Fauna and Flora (CITES).

- Documentation: Provide either in accordance with chain of custody certification scheme requirements:

  - Documentary evidence (which has been or can be independently verified) regarding the provenance of all timber supplied. or

  - Evidence that suppliers have adopted and are implementing a formal environmental purchasing policy for timber and wood-based products.

- Chain of Custody Certification scheme: Contractor's choice, in accordance with UK Government Timber Procurement Policy (UKTPP), i.e. FSC, GiB or PEFC

5 	Structural softwood

- Description: FOR STRUCTURAL USE GENERALLY

- Grading standard: To the appropriate BS EN 14081-1-compliant standard.

  - Grade: GS to BS 4978

- Strength class to BS EN 338: C24

- Treatment: Flame-retardant impregnation to NBS section Z12 and Wood Protection Association Commodity Specification FR2, Type INT2

10 	Ungraded softwood

- Description: FOR INTERNAL NONSTRUCTURAL USE

- Quality of timber: Free from decay, insect attack (except pinhole borers) and with no knots wider than half the width of the section.

- Treatment: Flame-retardant impregnation to NBS section Z12 and Wood Protection Association Commodity Specification FR1, Type INT2

30 	Selection and use of timber

- Timber members damaged, crushed or split beyond the limits permitted by their grading: Do not use.

32 	Notches, holes and joints in timber

- Notches and holes: Position in relation to knots or other defects so that the strength of members will not be reduced.

- Scarf joints, finger joints and splice plates: Do not use without approval.

35 	Processing treated timber

- Cutting and machining: Carry out as much as possible before treatment.

- Extensively processed timber: Retreat timber sawn lengthways, thicknessed, planed, ploughed, etc.

- Surfaces exposed by minor cutting/ drilling: Treat with two flood coats of a solution recommended by main treatment solution manufacturer.

40 	Moisture content

- Moisture content of wood and wood-based products at time of installation: Not more than:

  - Covered in generally unheated spaces: 24%.

  - Covered in generally heated spaces: 20%.

  - Internal in continuously heated spaces: 20%.

41 	Bolt/ screw assemblies

- Nuts and washers: Material grade and finish to suit bolts

- Washer dimensions: Diameter/ side length of washers in contact with timber faces to be minimum 3 times bolt diameter, with a thickness not less than 0.25 times bolt diameter.

43 	Bolted joints

- Bolt spacings (minimum): To BS EN 1995-1-1, section 8.5.

- Holes for bolts: Located accurately and drilled to diameters as close as practical to the nominal bolt diameter and not more than 2 mm larger.

- Washers: Placed under bolt heads and nuts that would otherwise bear directly on timber. Use spring washers in locations which will be hidden or inaccessible.

- Bolt tightening: So that washers just bite the surface of the timber. Ensure that at least one complete thread protrudes from the nut.

  - Checking: At agreed regular intervals. Tighten as necessary.

50 	Additional supports

- Provision: Position and fix additional studs, noggings and/ or battens to support edges of sheet materials, and wall/ floor/ ceiling-mounted appliances, fixtures, etc. shown on drawings.

- Material properties: Timber to be of adequate size and have the same treatment as adjacent timber supports.

55 	Joists generally

- Centres: Equal, and not exceeding designed spacing.

- Bowed joists: Installed with positive camber.

- End joists: Positioned about 50 mm from masonry walls.

60 	Joists on hangers

- Hangers: Bedded directly on and hard against supporting construction. Do not use packs or bed on mortar.

- Joists: Cut to leave not more than 6 mm gap at each end. Rebated to lie flush with underside of hangers.

- Fixing to hangers: A nail in every hole.

70 	Trimming openings

- Trimmers and trimming joists: Not less than 25 mm wider than general joists.

Ω End of Section

K10
Gypsum board dry linings/ partitions/ ceilings

To be read with preliminaries/ general conditions.

30 	Gypsum board wall lining systems Type 1

- Description: TYPE 1 - FIRE-RESISTING PARTITIONS (FR30)

- Manufacturer: British Gypsum

  - Contact details

    - Address: East Leake
Loughborough
Leicestershire
United Kingdom
LE12 6JU

    - Telephone: +44 (0)844 800 1991

    - Web: https://www.british-gypsum.com

    - Email: bg.technical@saint-gobain.com

  - Product reference: A206015 (B) MR2 (EN)

- Studs

  - Type: Gypframe 70 S 50 C Studs

  - Centres: 600 mm

  - Head condition: Structural steel floor deck.

  - Deflection allowance: 15 mm

- Fire performance

  - Reaction to fire: To BS EN 13501-1, Class B-s3, d2 or better

  - Fire resistance of complete assembly: To BS EN 13501-2, REI 30 or better

- Fire separation

  - Cavity fire barriers: As required.

- Insulation: Rock mineral wool to BS EN 13162;

  - Recycled content: Contractor's choice

  - Thickness: 50 mm

- Resilient layer: Not required

- Linings: First layer 12.5 mm plasterboard; face layer 12.5 mm moisture-resistant plasterboard

  - Recycled content: Submit proposals

  - Screw centres: As per manufacturers recommendations

- Finishing: Skim coat plaster

  - Primer/ Sealer: As recommended by board manufacturer for improved moisture resistance

- Accessories: Metal beads/ stops recommended by board manufacturer

- Other requirements: Fire-stopping around services as section P12

30 	Gypsum board wall lining systems Type 2

- Description: TYPE 2- FIRE-RESISTING PARTITIONS (FR30)

- Manufacturer: British Gypsum

  - Contact details

    - Address: East Leake
Loughborough
Leicestershire
United Kingdom
LE12 6JU

    - Telephone: +44 (0)844 800 1991

    - Web: https://www.british-gypsum.com

    - Email: bg.technical@saint-gobain.com

  - Product reference: A206015 (B) MR1 (EN)

- Studs

  - Type: Gypframe 70 S 50 C Studs

  - Centres: 600 mm

  - Head condition: Structural steel floor deck.

  - Deflection allowance: 15 mm

- Fire performance

  - Reaction to fire: To BS EN 13501-1, Class B-s3, d2 or better

  - Fire resistance of complete assembly: To BS EN 13501-2, REI 30 or better

- Fire separation

  - Cavity fire barriers: As required.

- Insulation: Rock mineral wool to BS EN 13162;

  - Recycled content: Contractor's choice

  - Thickness: 50 mm

- Resilient layer: Not required

- Linings: First layer 12.5 mm plasterboard; face layer 12.5 mm moisture-resistant plasterboard to inner side and double layer 12.5 mm plasterboard to outer side.

  - Recycled content: Submit proposals

  - Screw centres: As per manufacturers recommendations

- Finishing: Skim coat plaster

  - Primer/ Sealer: As recommended by board manufacturer for improved moisture resistance

- Accessories: Metal beads/ stops recommended by board manufacturer

- Other requirements: Fire-stopping around services as section P12

30 	Gypsum board wall lining systems Type 3

- Description: TYPE 3- FIRE-RESISTING PARTITIONS (FR30)

- Manufacturer: British Gypsum

  - Contact details

    - Address: East Leake
Loughborough
Leicestershire
United Kingdom
LE12 6JU

    - Telephone: +44 (0)844 800 1991

    - Web: https://www.british-gypsum.com

    - Email: bg.technical@saint-gobain.com

  - Product reference: A206015 (B) (EN)

- Studs

  - Type: Gypframe 70 S 50 C Studs

  - Centres: 600 mm

  - Head condition: Structural steel floor deck.

  - Deflection allowance: 15 mm

- Fire performance

  - Reaction to fire: To BS EN 13501-1, Class B-s3, d2 or better

  - Fire resistance of complete assembly: To BS EN 13501-2, REI 30 or better

- Fire separation

  - Cavity fire barriers: As required.

- Insulation: Rock mineral wool to BS EN 13162;

  - Recycled content: Contractor's choice

  - Thickness: 50 mm

- Resilient layer: Not required

- Linings: Double layer 12.5 mm plasterboard to both sides.

  - Recycled content: Submit proposals

  - Screw centres: As per manufacturers recommendations

- Finishing: Skim coat plaster

  - Primer/ Sealer: As recommended by board manufacturer for improved moisture resistance

- Accessories: Metal beads/ stops recommended by board manufacturer

- Other requirements: Fire-stopping around services as section P12

30 	Gypsum board wall lining systems Type 4

- Description: TYPE 4- FIRE-RESISTING PARTITIONS (FR60)

- Manufacturer: British Gypsum

  - Contact details

    - Address: East Leake
Loughborough
Leicestershire
United Kingdom
LE12 6JU

    - Telephone: +44 (0)844 800 1991

    - Web: https://www.british-gypsum.com

    - Email: bg.technical@saint-gobain.com

  - Product reference: A206016 (B) (EN)

- Studs

  - Type: Gypframe 70 S 50 C Studs

  - Centres: 600 mm

  - Head condition: Structural steel floor deck

  - Deflection allowance: 15 mm

- Fire performance

  - Reaction to fire: To BS EN 13501-1, Class B-s3, d2 or better

  - Fire resistance of complete assembly: To BS EN 13501-2, REI 30 or better

- Fire separation

  - Cavity fire barriers: As required.

- Insulation: Rock mineral wool to BS EN 13162;

  - Recycled content: Contractor's choice

  - Thickness: 50 mm

- Resilient layer: Not required

- Linings: Double layer 15 mm plasterboard to both sides.

  - Recycled content: Submit proposals

  - Screw centres: As per manufacturers recommendations

- Finishing: Skim coat plaster

  - Primer/ Sealer: As recommended by board manufacturer for improved moisture resistance

- Accessories: Metal beads/ stops recommended by board manufacturer

- Other requirements: Fire-stopping around services as section P12

Installation

60 	Ceilings

- Sequence: Fix boards to ceilings before installing dry lined walls and partitions.

- Orientation of boards: Fix with bound edges at right angles to supports and with ends staggered in adjacent rows.

- Two layer boarding: Stagger joints between layers.

61 	Metal framing for partitions/ wall linings

- Setting out: Accurately aligned and plumb.

  - Frame/ Stud positions: Equal centres to suit specified linings, maintaining sequence across openings.

  - Additional studs: To support vertical edges of boards.

- Fixing centres at perimeters (maximum): 600 mm.

- Openings: Form accurately.

  - Doorsets: Use sleeved or boxed metal studs and/ or suitable timber framing to achieve strength grade requirements for framing assembly and adequately support weight of door.

  - Services penetrations: Allow for associated fire-stopping.

62 	Metal furrings for wall linings

- Setting out: Accurately aligned and plumb.

  - Vertical furring positions: Equal vertical centres to suit specified linings, maintaining sequence across openings. Position adjacent to angles and openings.

  - Additional vertical furrings: To support vertical edges of boards and at junctions with partitions.

  - Horizontal furring positions: To provide continuous support to edges of boards.

- Adhesive bedding to furrings

  - Dabs: Length 200 mm (minimum). Located at ends of furrings and thereafter at 450 mm (maximum) centres.

  - Junctions with partitions: Continuous bed with no gaps across cavity.

65 	Dry lining generally

- General: Use fixing, jointing, sealing and finishing materials, components and installation methods recommended by board manufacturer.

- Standard:

- Gypsum plasterboard to BS EN 520.

- Gypsum fibre board to BS EN 15283-2.

- Evidence of compliance: Submit Declaration of Performance (DoP).

- Cutting gypsum boards: Neatly and accurately without damaging core or tearing paper facing.

- Cut edges: Minimize and position at internal angles wherever possible. Mask with bound edges of adjacent boards at external corners.

- Two layer boarding: Stagger joints between layers.

- Finishing: Neatly to give flush, smooth, flat surfaces free from bowing and abrupt changes of level.

67 	Skim coat plaster finish

- Plaster type: As recommended by board manufacturer

  - Thickness: 2-3 mm.

- Joints: Fill and tape except where coincident with metal beads.

- Finish: Tight, matt, smooth surface with no hollows, abrupt changes of level or trowel marks.

69 	Installing beads/ stops

- Cutting: Neatly using mitres at return angles.

- Fixing: Securely using longest possible lengths, plumb, square and true to line and level, ensuring full contact of wings with substrate.

- Finishing: After joint compounds/ plasters have been applied, remove surplus material while still wet from surfaces of beads exposed to view.

70 	Additional supports

- Framing: Accurately position and securely fix to give full support to:

  - Partition heads running parallel with, but offset from main structural supports.

  - Fixtures, fittings and service outlets. Mark framing positions clearly and accurately on linings.

  - Board edges and lining perimeters, as recommended by board manufacturer to suit type and performance of lining.

75 	New wet laid bases

- Dpcs: Install under full width of partitions/ freestanding wall linings.

  - Material: Bituminous sheet or plastics.

85 	Installing mineral wool insulation

- Fitting insulation: Closely butted joints and no gaps. Use fasteners to prevent slumping or displacement.

- Services

  - Electrical cables overlaid by insulation: Size accordingly.

  - Ceilings: Cut insulation around electrical fittings, etc.

86 	Cavity fire barriers within partitions/ Wall linings

- Metal framed systems

  - Material: Wire-reinforced mineral wool 50 mm (minimum) thick

  - Installation: Form accurately and fix securely with no gaps to provide a complete barrier to smoke and flame.

- Adhesive fixed wall lining systems

  - Material: Adhesive compound.

  - Installation: Form in a continuous line with no gaps to provide a complete barrier to smoke and flame.

87 	Sealing gaps and air paths

- Sealing: Apply sealant to perimeter abutments and around openings as a continuous bead with no gaps.

- Application: To clean, dry and dust free surfaces as a continuous bead with no gaps.

  - Gaps greater than 6mm between floor and underside of gypsum board: After sealing, fill with joint compound.

88 	Fire-stopping at perimeters of dry lining systems

- Material: Tightly packed mineral wool or intumescent mastic/ sealant.

- Application: To perimeter abutments to provide a complete barrier to smoke and flame.

89 	Cavity fire barriers within suspended ceilings

- Type: As recommended by board manufacturer to meet specified performance

- Fire resistance: To BS EN 13501-2, REI 30 or To BS EN 13501-2, EI 60 as required.

- Ceiling void subdivision: Fix barriers on line of partitions and not more than 40 m apart in any direction.

- Fixing at perimeters and joints: Secure, stable and continuous with no gaps, to provide a complete barrier to smoke and flame.

- Service penetrations: Cut and pack to maintain barrier integrity. Sleeve flexible materials. Adequately support services passing through barrier.

- Ceiling systems for fire protection: Do not impair fire-resisting performance of ceiling system.

90 	Seamless jointing

- Cut edges of boards: Lightly sand to remove paper burrs.

- Filling and taping: Fill joints, gaps and internal angles with jointing compound and cover with continuous lengths of tape, fully bedded.

- Protection of edges/ corners: Reinforce external angles, stop ends, etc. with specified edge/ angle bead.

- Finishing: Feather out jointing compound to give a flush, smooth, seamless surface.

- Nail/ screw depressions and minor indents: Fill with jointing compound to give a flush surface.

- Minor imperfections: Remove by light sanding.

91 	Vertical joints

- Joints: Centre on studs.

  - Partitions: Stagger joints on opposite sides of studs.

  - Two layer boarding: Stagger joints between layers.

92 	Horizontal joints

- Surfaces exposed to view: Horizontal joints not permitted. Seek instructions where height of partition/ lining exceeds maximum available length of board.

- Two layer boarding: Stagger joints between layers by at least 600 mm.

- Edges of boards: Support using additional framing.

  - Two layer boarding: Support edges of outer layer.

93 	Fixing gypsum board to metal framing/ Furrings

- Partitions/ Wall linings: Fix securely and firmly at the following centres (maximum):

  - Single layer boarding: To all framing at 300 mm centres. Reduce to 200 mm centres at external angles.

  - Multi-layer boarding: Face layer at 300 mm centres, and previous layers around perimeters at 300 mm centres.

- Ceilings: 230 mm. Reduce to 150 mm at board ends and at lining perimeters.

- Position of screws from edges of boards (minimum): 10 mm.

  - Screw heads: Set in a depression. Do not break paper or gypsum core.

94 	Fixing gypsum board to timber

- Fixing to timber: Securely at the following centres (maximum):

  - Nails: 150 mm.

  - Screws to partitions/ wall linings: 300 mm. Reduce to 200 mm at external angles.

  - Screws to ceilings: 230 mm.

- Position of nails/ screws from edges of boards (minimum)

  - Bound edges: 10 mm.

  - Cut/ unbound edges: 13 mm.

- Position of nails/ screws from edges of timber supports (minimum): 6 mm.

95 	Fixing gypsum board with adhesive dabs

- Setting out boards: Accurately aligned and plumb.

- Fixing to substrates: Securely using adhesive dabs.

- Adhesive dab spacings for each board

  - Horizontally: One row along top edge and one continuous dab along bottom edge.

  - Vertically: One row along each edge and thereafter at intermediate spacings to suit size of board:

    - 9.5 mm thick board, 1200 mm wide to have dab centres at 400 mm (min).

    - 9.5 or 12.5 mm thick board, 900 mm wide to have dab centres at 450 mm (min).

    - 12.5 mm thick board, 1200 mm wide to have dab centres at 600 mm (min).

- Adhesive dab dimensions (width x length): At least 50-75 mm x 250 mm.

  - Position of dabs from edges/ ends of boards (minimum): 25 mm.

Finishing

97 	Level of dry lining across joints

- Sudden irregularities: Not permitted.

- Joint deviations: Measure from faces of adjacent boards using methods and straightedges (450 mm long with feet/ pads) to BS 8212, clause 3.3.5.

  - Tapered edge joints

    - Permissible deviation (maximum) across joints when measured with feet resting on boards: 3 mm.

  - External angles

    - Permissible deviation (maximum) for both faces: 4 mm.

  - Internal angles

    - Permissible deviation (maximum) for both faces: 5 mm.

98 	Repairs to existing gypsum board

- Performance of repairs must match original specified performances.

- Filling small areas with broken cores: Cut away paper facing, remove loose core material and fill with jointing compound.

  - Finish: Flush, smooth surface suitable for redecoration.

- Large patch repairs: Cut out damaged area and form neat hole with rectangular sides. Replace with matching gypsum board.

  - Fixing: Use methods to suit type of dry lining, ensuring full support to all edges of existing and new gypsum board.

  - Finishing: Fill joints, tape and apply jointing compound to give a flush, smooth surface suitable for redecoration.

Ω End of Section

K40
Demountable suspended ceilings

To be read with preliminaries/ general conditions.

10 	Modular suspended ceilings - Generally Type A

- Ceiling system manufacturer: Rockfon

  - Contact details

    - Address: 14th Floor, Chiswick Tower
389 Chiswick High Road
London
United Kingdom
W4 4AL

    - Telephone: +44 (0)208 2227457

    - Web: https://www.rockfon.co.uk/

    - Email: fiona.ocallaghan@rockfon.com

  - Product reference: Rockfon® Artic™ (Artic E15 – 600 x 600 x 15 mm )

- Third-party certification: Cradle to Cradle Certified® Silver.

- Form: Infill unit.

- Rigidity: Rigid.

- Application: Ceiling mounting.

- Material: Stone wool.

- Acoustic performance

  - Purpose: Absorber.

- Fire performance

  - Reaction to fire: A1.

- Dimensions

  - Size (length x width): 600 x 600 mm.

  - Thickness (overall): 15 mm.

- Edges: E15.

- Finish: Nuanced.

- Colour: White.

10 	Modular suspended ceilings - Wet Areas Type B

- Ceiling system manufacturer: Rockfon

  - Contact details

    - Address: 14th Floor, Chiswick Tower
389 Chiswick High Road
London
United Kingdom
W4 4AL

    - Telephone: +44 (0)208 2227457

    - Web: https://www.rockfon.co.uk/

    - Email: fiona.ocallaghan@rockfon.com

  - Product reference: Rockfon® Koral™ (Koral A15 System T15 A,EECR - 600 x 600 x 15 mm)

- Third-party certification: Cradle to Cradle Certified® Silver.

- Form: Infill unit.

- Rigidity: Rigid.

- Application: Ceiling mounting.

- Material: Stone wool.

- Acoustic performance

  - Purpose: Absorber.

  - Sound absorption: Class A (to ISO 11654: 0.95 αw).

- Fire performance

  - Reaction to fire: A1 (to BS EN 13501-1).

- Dimensions

  - Size (length x width): 600 x 600 mm.

  - Thickness (overall): 15 mm.

- Profile: Geometric profile.

- Edges: A15.

10 	Modular suspended ceilings - Generally Type B

- Ceiling system manufacturer: Rockfon

  - Contact details

    - Address: 14th Floor, Chiswick Tower
389 Chiswick High Road
London
United Kingdom
W4 4AL

    - Telephone: +44 (0)208 2227457

    - Web: https://www.rockfon.co.uk/

    - Email: fiona.ocallaghan@rockfon.com

  - Product reference: Rockfon® Artic™ (Artic E15 – 600 x 600 x 15 mm )

- Third-party certification: Cradle to Cradle Certified® Silver.

- Form: Infill unit.

- Rigidity: Rigid.

- Application: Ceiling mounting.

- Material: Stone wool.

- Acoustic performance

  - Purpose: Absorber.

- Fire performance

  - Reaction to fire: A1.

- Dimensions

  - Size (length x width): 600 x 600 mm.

  - Thickness (overall): 15 mm.

- Edges: E15.

- Finish: Nuanced.

- Colour: White.

Components

31 	Standards

- Steel panels: To BS EN 10346.

- Aluminium sheet, strip and plate: To BS EN 485-1 and -2.

- Aluminium bars, tubes and sections: To relevant parts of BS EN 515, BS EN 573, BS EN 755 and BS EN 12020.

Execution

40 	Workmanship generally

- Fixing: Secure. In accordance with manufacturers' recommendations and in accordance with BS EN 13964. Provide additional bracing and stiffening to give a stable ceiling system.

- Setting out: Accurate. Provide level soffits free from undulations and lipping.

- Infill and access units, integrated services: Fitted correctly and aligned.

- Lines and joints: Straight and parallel to walls, unless specified otherwise.

- Edge infill units size (minimum): Half standard width or length.

- Corner infill units size (minimum): Half standard width and length.

- Grid: Position to suit infill unit sizes. Allow for permitted deviations from nominal sizes of infill units.

- Infill joints and exposed suspension members: Straight, aligned and parallel to walls, unless specified otherwise.

- Suitability of construction: Give notice where building elements and features to which the ceiling systems relate are not square, straight or level.

50 	Installing hangers

- General: Straighten and tension before use.

- Installation: Install vertical without bends or kinks. Do not allow hangers to press against fittings, services, or insulation covering ducts/ pipes.

- Obstructions: Where obstructions prevent vertical installation, either brace diagonal hangers against lateral movement, or hang ceiling system on an appropriate rigid sub-grid bridging across obstructions and supported to prevent lateral movement.

- Extra hangers: Provide as necessary to carry additional loads.

- Fixing

  - Wire hangers: Tie securely at top and bottom with tight bends to loops to prevent vertical movement.

  - Angle/ Strap hangers: Do not use rivets for top fixing.

51 	Installing perimeter trims

- Jointing: Neat and accurate, without lipping or twisting.

  - External and internal corners: Mitre joints generally. Overlap joints at internal corners are not acceptable.

  - Intermediate butt joints: Minimize. Use longest available lengths of trim. Align adjacent lengths.

- Fixing: Fix firmly to perimeter wall, edge battens or other building structure.

  - Fixing centres: 450 mm

52 	Installing board-suspended ceiling systems

- Cut boards: Neat and accurate.

- Fixing to grid

  - Board edges: Fully support. Screw to grid members. Set heads of screws below surface of boards and fill flush with surface.

  - Boards applied in two or more layers: Stagger joints.

- Movement joints: Provide as appropriate for the area of ceiling system and/ or to coincide with movement joints in surrounding structure.

53 	Openings in ceiling materials

- General: Neat and accurate. To suit sizes and edge details of fittings. Do not distort ceiling system.

57 	Ceiling systems intended for fire protection

- Junctions of ceiling systems with perimeter abutments and service penetrations: Seal gaps with tightly packed mineral wool or intumescent sealant to prevent penetration of smoke and flame

- Ceiling system/ Wall junctions: Maintain protective value of ceiling system.

- Fixings and grounds: Non-combustible.

- Metal trim: Provide for thermal expansion.

- Access and access panels: Maintain continuity of fire protection.

60 	Cavity fire barriers

- Material: Wire-reinforced mineral wool pads

  - Thickness: To give same fire resistance as ceiling.

- Fixing: Accurate. Secure with no gaps. Provide a complete barrier to smoke and flame.

- Do not impair fire-resisting performance of ceiling system.

- Fixing: Secure barrier at head and base using proprietary angle support system

  - General: Fix battens securely to channels or angles at abutments to building structure.

  - At perimeters and joints: Provide permanent stability and continuity, with no gaps, to form a complete barrier to smoke and flame.

- Joints: Form to preserve integrity in fire.

- Service penetrations: Cut barriers neatly to accommodate services. Fit fire-resistant sleeves around flexible materials. Fill gaps around services to fire barrier manufacturer's recommendations to maintain barrier integrity. Adequately support services passing through the barrier.

- Ceiling systems intended for fire protection: Do not impair fire-resisting performance of ceiling system.

- Ceiling systems not intended for fire protection: Do not mechanically interlink barriers with ceiling system.

65 	Integrated services

- General: Position services accurately, support adequately. Align and level in relation to the ceiling and suspension system. Do not diminish performance of ceiling system.

- Small fittings: Support with rigid backing boards or other suitable means. Do not damage or distort the ceiling.

  - Reaction to fire rating of additional supporting material: Not less than ceiling material.

- Services outlets

  - Supported by ceiling system: Provide additional hangers.

  - Independently supported: Provide flanges to support ceiling system.

66 	Ceiling-mounted luminaires

- Support: By ceiling system

  - Ceiling supported luminaires: Modifications and/ or extra support required: To each luminaire.

  - Independently supported luminaires: Suspension adjusted to line and level of ceiling.

- Surface mounted luminaires: Units installed so that in the event of fire, the designed grid expansion provision is not affected.

- Modular fluorescent recessed luminaires: Compatible with ceiling module. Extension boxes must not foul ceiling system.

- Recessed rows of luminaires: Provide flanges for support of grid and infill units, unless mounted above grid flanges. Retain in position with lateral restraint.

- Fire-protecting/ resisting ceiling systems: Luminaires must not diminish protection integrity of ceiling system.

- Access: Provide access for maintenance of luminaires.

67 	Mechanical services

- Fan coil units

  - Inlet and outlet grilles: Trim ceiling grid and infill units to suit.

  - Space beneath: Sufficient for ceiling system components.

  - Suspension and connections: Permit accurate setting out and levelling of fan coil units.

- Air grilles and diffusers

  - Setting out: Accurate and level.

  - Linear air diffusers: Retain in place with lateral restraint. Provide flanges for support of grid and infill units.

  - Grille/ diffuser ceiling joints: Provide smudge rings and edge seals.

- Smoke detectors and PA speakers

  - Ceiling infill units: Scribe and trim to suit.

  - Independent suspension: Not required

  - Flexible connections: Required.

- Sprinkler heads: Carefully set out and level.

Completion

85 	Spares

- General: At practical completion, supply the following: 20 tiles for K40/10 Type A ceiling system and 10 tiles for K40/10 Type B ceiling system.

Ω End of Section

L20
Doors/ shutters/ hatches

To be read with preliminaries/ general conditions.

10 	Timber procurement

- Timber (including timber for wood-based products): Obtained from well-managed forests and/ or plantations in accordance with:

  - The laws governing forest management in the producer country or countries.

  - International agreements such as the Convention on International Trade in Endangered Species of wild fauna and flora (CITES).

- Documentation: Provide either in accordance with chain of custody certification scheme requirements:

  - Documentary evidence (which has been or can be independently verified) regarding the provenance of all timber supplied; or

  - Evidence that suppliers have adopted and are implementing a formal environmental purchasing policy for timber and wood-based products.

55 	Doorsets

- Description: INTERNAL

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Standard: to BS EN 16034

- Finish as delivered: Factory-applied primer

- Glazing/ infill details: Clear fire-resisting glazing

  - Manifestation: Not required

  - Beading: Internal

- Ironmongery: As ironmongery schedule

- Perimeter seals: Fire and smoke seal

- Thermal performance (U-value maximum): Manufacturer's standard

- Fire performance

  - Fire resistance: To BS EN 13501-2, EIW 30S

  - Smoke leakage: Manufacturer's standard

  - Reaction to fire: To BS EN 13501-1, Class B or better

- Other requirements: None

- Fixing: Plugged and screwed

  - Spacing of fixings (frames not predrilled): Maximum 150 mm from ends of each jamb and at 600 mm maximum centres.

- Verification: Full door schedule

  - Submittals: Full door schedule and specification

  - Timing: With tender submission

70 	Fire and smoke resistance

- Requirement: Specified performance to be the minimum period attained when tested for integrity in accordance with BS 476-22, BS EN 1634-1 or BS EN 1634-3.

- Components and assemblies will be marked to the relevant product standard and/ or third-party certification rating.

75 	Fire-resisting/ smoke control doors/ doorsets

- Gaps between frames and supporting construction: Filled as necessary in accordance with door/ doorset manufacturer's instructions.

80 	Sealant joints

- Sealant

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Colour: To be agreed.

  - Application: As section Z22 to prepared joints. Triangular fillets finished to a flat or slightly convex profile.

85 	Fixing ironmongery generally

- Fasteners: Supplied by ironmongery manufacturer.

  - Finish/ Corrosion resistance: To match ironmongery.

- Holes for components: No larger than required for satisfactory fit/ operation.

- Adjacent surfaces: Undamaged.

- Moving parts: Adjusted, lubricated and functioning correctly at completion.

Ω End of Section

M10
Cement based levelling/ wearing screeds

To be read with preliminaries/ general conditions.

12 	Smoothing and levelling underlay compounds Type A

- Screed manufacturer: Ball, F and Co Ltd

  - Contact details

    - Address: Churnetside Business Park
Station Road
Cheddleton
Leek
Staffordshire
ST13 7RS

    - Telephone: +44 (0)1538 361633

    - Web: www.f-ball.com

    - Email: mail@f-ball.co.uk

  - Product reference: Stopgap 1200

- Material: Cementitious.

- Standards: To EN 13813:2002.

- Working time: 15–20 minutes at +20°C.

- Setting time: 60 minutes at +20°C.

- Cure time: At 3 mm ready to receive most floorcoverings: 4 hours.

- Consumption (per layer applied): 1.98 kg/m² per mm thickness.

- Compressive strength - 1 day: >6.0 N/mm².

- Compressive strength - 7 days: >10.0 N/mm².

- Compressive strength - 28 days: >16.0 N/mm².

- Flexural strength: 1 Day: >2.0 N/mm²; 7 Days: >4.0 N/mm²; 28 Days: >6.0 N/mm².

21 	Suitability of substrates

- General

  - Suitable for specified levels and flatness/ regularity of finished surfaces. Consider permissible minimum and maximum thicknesses of screeds.

  - Sound and free from significant cracks and gaps.

- Concrete strength: In accordance with BS 8204-1, Table 2.

- Cleanliness: Remove plaster, debris and dirt.

- Moisture content: To suit screed type. New concrete slabs to receive fully or partially bonded construction must be dried out by exposure to the air for minimum six weeks.

22 	Proprietary levelling/wearing screeds

- General: Materials, mix proportions, mixing methods, minimum/ maximum thicknesses and workmanship must be in accordance with recommendations of screed manufacturer.

- Standard: In accordance with BS 8204-3

47 	Admixtures

- Standards; In accordance with BS 8204-1, Table 1.

- Calcium chloride: Do not use in admixtures.

50 	Mixing

- Water content: Minimum necessary to achieve full compaction, low enough to prevent excessive water being brought to surface during compaction..

- Mixing: Mix materials thoroughly to uniform consistency in a suitable forced action mechanical mixer. Do not use a free fall drum type mixer.

- Consistency: Use while sufficiently plastic for full compaction.

- Ready-mixed retarded screed mortar: Use within working time and site temperatures recommended by manufacturer. Do not retemper.

52 	Compaction

- General: Compact thoroughly over entire area.

- Screeds over 50 mm thick: Lay in two layers of equal thickness. Roughen surface of compacted lower layer then immediately lay upper layer.

55 	Joints in levelling screeds

- Laying screeds: Lay continuously using 'wet screeds' between strips or bays. Minimize defined joints.

- Daywork joints: Form with vertical edge.

70 	Smooth floated finish

- Finish: Even texture with no ridges or steps.

75 	Trowelled finish to levelling screeds

- Floating: To an even texture with no ridges or steps.

- Trowelling: To a uniform smooth surface, free from trowel marks and other blemishes, and suitable to receive specified flooring material.

80 	Trowelled finish to wearing screeds

- Floating: To an even texture with no ridges or steps.

- Trowelling: Successively trowel at intervals, applying sufficient pressure to close surface and give a uniform, smooth finish free from trowel marks and other blemishes.

85 	Finishing generally

- Timing: Carry out all finishing operations at optimum times in relation to setting and hardening of screed material.

- Prohibited treatments to screed surfaces

  - Wetting to assist surface working.

  - Sprinkling cement.

90 	Curing

- General: Prevent premature drying. Immediately after laying, protect surface from wind, draughts and strong sunlight. As soon as screed has set sufficiently, closely cover with polyethylene sheeting.

- Curing period (minimum): As soon as screed has set sufficiently, closely cover with polyethylene sheeting for period recommended by screed manufacturer.

- Drying after curing: Allow screeds to dry gradually. Do not subject screeds to artificial drying conditions that will cause cracking or other shrinkage related problems.

Ω End of Section

M20
Plastered/ rendered/ roughcast coatings

To be read with preliminaries/ general conditions.

50 	Gypsum plaster skim coat on plasterboard

- Plasterboard: 12.5 mm On metal resilient (acoustic) bars

  - Preparation: Bonding agent recommended by plaster manufacturer

- Plaster: Board finish/ plaster to BS EN 13279-1, class B.

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Thickness: 2-5 mm

  - Finish: Smooth.

60 	Cements for mortars

- Cement: To BS EN 197-1.

  - Types: Portland cement, CEM I.

- Portland slag cement, CEM II.

- Portland fly ash cement, CEM II.

  - Strength class: 32.5, 42.5 or 52.5.

- Sulfate resisting cement: To BS EN 197-1.

61 	Lime for cement gauged mortars

- Standard: To BS EN 459-1.

  - Type: CL 90S.

62 	Admixtures for cement gauged mortars

- Suitable admixtures: Select from:

  - Air entraining (plasticizing) admixtures: To BS EN 934-2 and compatible with other mortar constituents.

  - Other admixtures: Submit proposals.

- Prohibited admixtures: Calcium chloride and admixtures containing calcium chloride.

63 	Sand for cement gauged mortars

- Standard: To BS EN 13139.

  - Grading: 0/2 or 0/4 (CP or MP); category 2 fines.

- Colour and texture: Consistent. Obtain from one source.

65 	Mixing

- Render mortars (site-made)

  - Batching: By volume using gauge boxes or buckets.

  - Mix proportions: Based on damp sand. Adjust for dry sand.

  - Lime:sand: Mix thoroughly. Allow to stand, without drying out, for at least 16 hours before using.

- Mixes: Of uniform consistence and free from lumps.

- Contamination: Prevent intermixing with other materials.

67 	Cold weather

- General: Do not use frozen materials or apply coatings on frozen or frost bound substrates.

- Internal work: Take precautions to prevent damage to internal coatings when air temperature is below 3°C.

- External work: Avoid when air temperature is at or below 5°C and falling or below 3°C and rising.

69 	Ready prepared lime putty

- Type: Slaked directly from CL 90 quicklime to BS EN 459-1, using an excess of water.

  - Maturation: In pits/ containers that allow excess water to drain away.

  - Density of matured lime putty: 1.3-1.4 kg/L.

- Maturation period before use (minimum): 90 days.

- Storage: Prevent drying out or wetting. Protect from frost.

71 	Suitability of substrates

- General: Suitable to receive coatings. Sound, free from contamination and loose areas.

- Cutting, chasing, making good, fixing of conduits and services outlets and the like: Completed.

- Tolerances: Permitting specified flatness/ regularity of finished coatings.

- Cleanliness: Free from dirt, dust, efflorescence and mould, and other contaminants incompatible with coatings.

74 	Existing damp affected plaster/ render

- Plaster affected by rising damp: Remove to a height of 300 mm above highest point reached by damp or 1 m above dpc, whichever is higher.

- Perished and salt contaminated masonry

  - Mortar joints: Rake out.

  - Masonry units: Submit proposals.

- Drying out substrates: Establish drying conditions.

- Faults in substrate (structural deficiencies, additional sources of damp, etc.): Submit proposals.

76 	Removing defective existing plaster

- Plaster for removal: Loose, hollow, soft, friable, badly cracked, affected by efflorescence or otherwise damaged.

  - Hollow, detached areas: Obtain instructions

- Stained plaster: Remove

- Removing defective plaster: Cut back to a square, sound edge.

- Faults in substrate (structural deficiencies, additional sources of damp, etc.): Submit proposals.

- Cracks

  - Fine hairline cracking/ crazing: Leave.

  - Other cracks: Cut out to a width of 75 mm (minimum)

- Dust and loose material: Remove from exposed substrates and edges.

78 	Removing defective existing render

- Render for removal: Detached, hollow, soft, friable, badly cracked, affected by efflorescence or otherwise damaged.

- Removing defective render: Cut out to regular rectangular areas with straight edges.

  - Horizontal and vertical edges: Square cut or slightly undercut.

  - Bottom edges to external render: Do not undercut.

  - Render with imitation joints: Cut back to joint lines.

- Cracks (other than hairline cracks): Cut out to a width of 75 mm (minimum).

- Dust and loose material: Remove from exposed substrates and edges.

80 	plasterboard backings

- Fixings, accessories and installation methods: As recommended by board manufacturer.

- Fixing: At the following centres (maximum):

  - Nails: 150 mm.

  - Screws to partitions/ walls: 300 mm. Reduce to 200 mm at external angles.

  - Screws to ceilings: 230 mm.

- Position of nails/ screws from edges of boards (minimum)

  - Bound edges: 10 mm.

  - Cut/ unbound edges: 13 mm.

- Position of nails/ screws from edges of supports (minimum): 6 mm.

- Nail/ screw heads: Set below surface. Do not break paper or gypsum core.

- Additional framing supports

  - Fixtures, fittings and service outlets: Accurately position to suit fasteners.

  - Board edges and perimeters: To suit type and performance of board.

- Joints

  - Ceilings

    - Bound edges: At right angles to supports and with ends staggered in adjacent rows.

    - Two layer boarding: Stagger joints between layers.

  - Partitions/ walls

    - Vertical joints: Centre on studs. Stagger joints on opposite sides of studs.

    - Two layer boarding: Stagger joints between layers.

    - Horizontal joints:

    - Two layer boarding: Stagger joints between layers by at least 600 mm. Support edges of outer layer.

  - Joint widths (maximum): 3 mm.

  - End joints: Stagger between rows.

  - Two layer boarding: Stagger joints between layers.

- Joint reinforcement tape: Apply to joints and angles except where coincident with metal beads.

81 	Beads/ stops for internal use

- Standard: In accordance with BS EN 13914-2.

- Material: Stainless steel to BS EN 13658-1

82 	Beads/ stops for external use

- Standard: In accordance with BS EN 13914-1.

- Materials: Stainless steel to BS EN 13658-2

- Fixing: Secure and true to line and level.

  - Beads/ stops to external render: Fix mechanically.

86 	Crack control at junctions between dissimilar solid substrates

- Locations: Where defined movement joints are not required. Where dissimilar solid substrate materials are in same plane and rigidly bonded or tied together.

- Crack control materials

  - Isolating layer: Building paper to BS 1521.

  - Metal lathing: Externally: Stainless steel ribbed expanded metal.
Internally: Galvanized steel plain expanded metal with spacers

- Installation: Fix metal lathing over isolating layer. Stagger fixings along both edges of lathing.

- Width of installation over single junctions

  - Isolating layer: 150 mm.

  - Lathing: 300 mm.

- Width of installation across face of dissimilar substrate material (column, beam, etc. with face width not greater than 450 mm)

  - Isolating layer: 25 mm (minimum) beyond junctions with adjacent substrate.

  - Lathing: 100 mm (minimum) beyond edges of isolating layer.

87 	Application of coatings

- General: Apply coatings firmly and achieve good adhesion.

- Appearance of finished surfaces: Even and consistent. Free from rippling, hollows, ridges, cracks and crazing.

  - Accuracy: Finish to a true plane, to correct line and level, with angles and corners to a right angle unless specified otherwise, and with walls and reveals plumb and square.

- Drying out: Prevent excessively rapid or localized drying out.

- Keying undercoats: Cross scratch plaster coatings and comb render coatings. Do not penetrate undercoat.

94 	Flatness/ surface regularity

- Sudden irregularities: Not permitted.

- Deviation of plaster surface: Measure from underside of a straight edge placed anywhere on surface.

  - Permissible deviation (maximum) for plaster not less than 13 mm thick: 3 mm in any consecutive length of 1800 mm.

Ω End of Section

M40
Stone/ concrete/ quarry/ ceramic tiling/ mosaic

To be read with preliminaries/ general conditions.

5 	Tiling to Showers and WHB Splashbacks

- Tiles: 100 x 200mm white ceramic gloss bevel edge metro wall tiles

  - Manufacturer/ Supplier: Submit proposals

    - Product reference: Submit proposals

  - Colour: White

  - Finish: Gloss

    - Ceramic tiles: Glazed

  - Size: 100 x 200 mm

  - Slip potential

    - Slip resistance value (SRV) (minimum)/ Pendulum test value (PTV) (minimum) to BS 7976-1, -2 and -3: Manufacturer’s standard

    - Surface roughness (Rz) (minimum) in accordance with BS 1134: Manufacturer’s standard

    - Ramp test class: Manufacturer’s standard

  - Recycled content: Contractor’s choice

  - Other requirements: None

- Bedding

  - Walls: Adhesive bed notched trowel method, as clause 50

  - Adhesive to BS EN 12004-1: Contractor’s choice

- Joint width: As spacer lugs

- Grout: Mapei Ultracolour Plus Black

15 	New backgrounds/ bases

- Background drying times (minimum)

  - Brick/block walls: six weeks.

  - Rendering: two weeks.

  - Gypsum plaster: four weeks.

- Base drying times (minimum)

  - Concrete slabs: six weeks.

  - Cement:sand screeds: three weeks.

20 	Existing backgrounds/ bases generally

- Efflorescence, laitance, dirt, loose and defective material: Remove and make good defective areas with materials compatible with background/base and bedding.

- Deposits of oil, grease and other materials incompatible with the bedding: Remove.

- Tile, paint and other nonporous surfaces: Clean.

- Wet backgrounds: Dry before tiling.

- Paint with unsatisfactory adhesion: Remove so as not to impair bedding adhesion.

25 	New plaster

- Plaster: Dry, solidly bedded, free from dust and friable matter.

- Plaster primer: Apply if recommended by adhesive manufacturer.

30 	Fixing generally

- Colour/ shade: Avoid unintended variations within tiles for use in each area/ room.

  - Variegated tiles: Mix thoroughly.

- Adhesive: Compatible with background/ base.

- Cut tiles: Neat and accurate.

- Fixing: Provide adhesion over entire background/ base and tile backs.

- Final appearance: Before bedding material sets, make adjustments necessary to give true, regular appearance to tiles and joints.

- Deviation of surface: Measure from underside of a 2 m straightedge with 3 mm thick feet placed anywhere on surface. The straightedge should not be obstructed by the tiles/ mosaics and no gap should be greater than 6 mm, i.e. a tolerance of

- Surplus bedding material: Clean from joints and face of tiles/ mosaics.

32 	Mortar bedding

- Bedding mix

  - Cement: Portland to BS EN 197-1, type CEM I/42.5.

  - Sand for walls: Fine aggregate to BS EN 13139.

    - Grading designation: 0/2 (CP or MP) category 2 fines.

  - Sand for floors: Fine aggregate to BS EN 13139.

- Grading designation: 0/4 (MP) category 1 fines and between 20-66% passing a 0.5 sieve.

- Batching: Select from:

  - Batch by weight.

  - Batch by volume: Permitted on the basis of previously established weight:volume relationships of the particular materials. Use accurate gauge boxes. Allow for bulking of damp sand.

- Mixing: Mix materials thoroughly to uniform consistence. Use a suitable forced action mechanical mixer. Do not use a free fall type mixer.

- Application: At normal temperatures use within two hours. Do not use after initial set. Do not retemper.

35 	Setting out

- Joints: True to line, continuous and without steps.

  - Joints on walls: Horizontal, vertical and aligned round corners.

  - Joints in floors: Parallel to main axis of space or specified features.

- Cut tiles: Minimize number, maximize size and locate unobtrusively.

- Joints in adjoining floors and walls: Align.

- Joints in adjoining floors and skirtings: Align.

- Movement joints: Where locations are not indicated, submit proposals.

50 	Adhesive bed – notched trowel method to walls

- Application: By 3 mm floated coat of adhesive to dry background. Comb surface.

- Tiling: Press tiles firmly onto float coat.

55 	Adhesive bed – notched trowel and buttering method to walls

- Application: By floated coat of adhesive to dry background. Comb surface.

- Tiling: Apply thin even coat of adhesive to backs of dry tiles. Fill any profiles. Press tiles firmly onto float coat.

- Finished adhesive thickness: 3 mm or within the range allowed by the adhesive manufacturer.

57 	Adhesive bed – buttering method

- Tiling: Apply even coat of adhesive to backs of dry tiles. Fill any ribbed, deep keyed or button profiles.

- Finished adhesive thickness

  - Walls: 3 mm or within the range allowed by the adhesive manufacturer.

  - Floors: Within the range allowed by the adhesive manufacturer.

70 	Grouting

- Sequence: Grout when bed/ adhesive has set sufficient to prevent disturbance of tiles.

- Joints: 6 mm deep (or depth of tile if less). Free from dust and debris.

- Grouting: Fill joints completely, tool to profile, clean off surface. Leave free from blemishes.

- Profile: Slightly concave

- Polishing: When grout is hard, polish tiling with dry cloth.

Ω End of Section

M50
Rubber/ plastics/ cork/ lino/ carpet tiling/ sheeting

To be read with preliminaries/ general conditions.

15 	Pile carpet tiles Type A

- Carpet tiles to BS EN 14041 and BS EN 1307

  - Manufacturer: Burmatex Ltd

    - Contact details

      - Address: Victoria Mills
The Green
Ossett
West Yorkshire
United Kingdom
WF5 0AN

      - Telephone: +44 (0)1924 262525

      - Web: https://www.burmatex.co.uk

      - Email: marketing@burmatex.co.uk

    - Product reference: tivoli® - carpet tiles (tivoli®)

  - Style: Solid colour loop pile carpet tile.

  - Material: Nylon.

  - Classification

    - Standard: To BS EN 1307.

    - Third-party certification: BSI and UKAS certified.

    - Level of use class: To BS EN 1307, class 33.

    - Luxury rating class: LC2.

  - Recycled content: 50% (minimum) to BS EN ISO 14021.

  - Size: 500 x 500 mm.

  - Colour and pattern: 20275 aruba dusk.

  - Design: Monolithic.

  - Weight: 4050 g/m².

  - Thickness: 6.5 mm.

  - Flammability: Euroclass Bfl-s1.

  - Castor chair rating (to BS EN 985): Pass.

  - Static loading (to BS 4939:1987 (2003)): Recovery >80% (24 hours).

  - Dynamic loading (to BS ISO 2094:1999 (2005)): Loss <20% (1000 impacts).

  - Static electricity: Body voltage test (to BS ISO 6356:2000): <2 kV.

  - Sound performance: Reduction in impact noise (to BS EN 140-8:1998): 23 dB.

  - Colour fastness: Light (to BS EN ISO 105 – BO2): grade 6 (minimum); shampoo (to BS 1006: UK-TB:1990): grade 4–5 (minimum).

  - Thermal resistance: Tog rating 0.39; ISO 8302: 0.04 m²K/W.

  - Environmental specifics: EPD-assessed.

20 	Particle-based enhanced slip-resistant polyvinyl chloride (PVC) sheets Type A

- Flooring roll

  - Manufacturer: Polyflor Ltd

    - Contact details

      - Address: PO Box 3
Radcliffe New Road
Whitefield
Manchester
M45 7NR

      - Telephone: +44 (0)161 767 1122

      - Web: https://www.polyflor.com/

      - Email: info@polyflor.com

    - Product reference: Polysafe Standard PUR Safety Flooring (Twilight)

  - Standard: To BS EN 13845.

  - Use class: To BS EN ISO 10874, class 23, 34 and 43.

  - Slip potential

    - Slip resistance value (SRV) (minimum)/ Pendulum test value (PTV) (minimum): R10. 36 + Pendulum Wet Test (4S Rubber/Slider 96).

    - Surface roughness (Rz) (minimum): ≥20 μm.

  - Width: 2000 mm.

  - Thickness: 2 mm.

  - Colour and pattern: Twilight.

  - Acoustic underlay: Acoustifoam.

40 	Laying coverings on new wet laid bases

- Base drying aids: Not used for at least four days prior to moisture content test.

- Base moisture content test: Carry out in accordance with BS 5325, Annexe A or BS 8203, Annexe A.

- Commencement of laying coverings: Not until all readings show 75% relative humidity or less.

45 	Existing floor covering removed

- Substrate: Clear of covering and as much adhesive as possible. Skim with smoothing compound to give smooth, even surface.

60 	Setting out tiles

- Method: Set out from centre of area/ room so that wherever possible:

  - Tiles along opposite edges are of equal size.

  - Edge tiles are more than 50% of full tile width.

65 	Laying coverings

- Base/ substrate condition: Rigid, dry, smooth, free from grease, dirt and other contaminants.

- Use a primer where recommended by adhesive manufacturer. Allow to dry thoroughly.

- Adhesive: As specified, as recommended by covering manufacturer or, as approved.

- Conditioning of materials prior to laying: As recommended by manufacturer.

- Environment: Before, during and after laying, provide adequate ventilation and maintain temperature and humidity approximately at levels which will prevail after building is occupied.

- Finished coverings: Accurately fitted, tightly jointed, securely bonded, smooth and free from air bubbles, rippling, adhesive marks, stains, trowel ridges and high spots.

70 	Edgings and cover strips

- Manufacturer: Submit proposals

  - Product reference:  Submit proposals

- Material/ finish: Aluminium

- Fixing: Secure (using matching fasteners where exposed to view) with edge of covering gripped.

85 	Waste

- Spare covering material: Retain suitable material for patching. On completion submit pieces for selection. Hand over selected pieces to Employer.

Ω End of Section

M60
Painting/ clear finishing

To be read with preliminaries/ general conditions.

14 	Emulsion Paint - New Woodwork/MDF Type A

- Manufacturer: Dulux Trade, brand of AkzoNobel

  - Contact details

    - Address: AkzoNobel Decorative Paints
Wexham Road
Slough
Berkshire
United Kingdom
SL2 5DS

    - Telephone: +44 (0)333 222 7070

    - Web: https://www.duluxtradepaintexpert.co.uk/en

    - Email: project.support@akzonobel.com

  - Product reference: Quick Dry Satinwood

- Composition: Modified acrylic.

- Sheen: Satin.

- Colour: RAL 7035

- System code: D1334S – Internal MDF/ Internal non resinous softwood/ Hardwood.

- Form: Liquid.

- Coverage: 12 m²/L.

- Viscosity: 12,68 cm²/s.

14 	Emulsion Paint - Walls Type B

- Manufacturer: Dulux Trade, brand of AkzoNobel

  - Contact details

    - Address: AkzoNobel Decorative Paints
Wexham Road
Slough
Berkshire
United Kingdom
SL2 5DS

    - Telephone: +44 (0)333 222 7070

    - Web: https://www.duluxtradepaintexpert.co.uk/en

    - Email: project.support@akzonobel.com

  - Product reference: Dulux Trade Diamond Eggshell.

- Composition: Acrylic copolymer.

- Sheen: Eggshell.

- Colour: RAL 000 9002

- System code: D597 – New plaster/ plasterboard.

- Form: Liquid.

22 	Handling and storage

- Coating materials: Deliver in sealed containers, labelled clearly with brand name, type of material and manufacturer's batch number.

- Materials from more than one batch: Store separately. Allocate to distinct parts or areas of the work.

28 	Protection

- 'Wet paint' signs and barriers: Provide where necessary to protect other operatives and general public, and to prevent damage to freshly applied coatings.

30 	Preparation generally

- Standard: In accordance with BS 6150.

- Refer to any pre-existing CDM Health and Safety File and CDM Construction Phase Plan where applicable.

- Risk assessments and method statements for suspected hazardous materials: Prepare for operations, disposal of waste, containment and reoccupation, and obtain approval before commencing work.

- Preparation materials: Types recommended by their manufacturers and the coating manufacturer for the situation and surfaces being prepared.

- Substrates: Sufficiently dry in depth to suit coating.

- Efflorescence salts, dirt, grease and oil: Remove. Give notice if contamination of surfaces/ substrates has occurred.

- Surface irregularities: Provide smooth finish.

- Organic growths and infected coatings

  - Remove with assistance of biocidal solution.

  - Apply residual effect biocidal solution to inhibit regrowth.

- Joints, cracks, holes and other depressions: Fill with stoppers/ fillers. Provide smooth finish.

- Dust, particles and residues from preparation: Remove and dispose of safely.

- Water-based stoppers and fillers

  - Apply before priming unless recommended otherwise by manufacturer.

  - If applied after priming: Patch prime.

- Doors, opening windows and other moving parts

  - Ease, if necessary, before coating.

  - Prime resulting bare areas.

32 	Previously coated surfaces generally

- Preparation: In accordance with BS 6150.

- Contaminated or hazardous surfaces: Give notice of:

  - Coatings suspected of containing lead.

  - Substrates suspected of containing asbestos or other hazardous materials.

  - Significant rot, corrosion or other degradation of substrates.

- Risk assessment and method statement for hazardous materials: Prepare for operations, disposal of waste, containment and reoccupation, and obtain approval before commencing work.

- Removing coatings: Do not damage substrate and adjacent surfaces or adversely affect subsequent coatings.

- Loose, flaking or otherwise defective areas: Carefully remove to a firm edge.

- Alkali affected coatings: Completely remove.

- Retained coatings

  - Thoroughly clean.

  - Gloss-coated surfaces: Provide key.

- Partly removed coatings

  - Apply additional preparatory coats.

  - Junctions: Provide flush surface.

- Completely stripped surfaces: Prepare as for uncoated surfaces.

35 	Fixtures and fittings

- Risk assessment and method statement for hazardous materials: Prepare for operations, disposal of waste, containment and reoccupation, and obtain approval before commencing work.

- Removal: Before commencing work: Ironmongery, cover plates, grilles, wall clocks, and other surface mounted fixtures.

- Replacement: Refurbish as necessary, refit when coating is dry.

36 	Ironmongery

- Removal: Before commencing work remove ironmongery from surfaces to be coated.

- Hinges: Remove

- Replacement: Refurbish as necessary; refit when coating is dry.

37 	Wood preparation

- General: Provide smooth, even finish with lightly rounded arrises.

- Degraded or weathered surface wood: Take back surface to provide suitable substrate.

- Degraded substrate wood: Repair with sound material of same species.

- Heads of fasteners: Countersink sufficient to hold stoppers/ fillers.

- Resinous areas and knots: Apply two coats of knotting.

- Defective primer: Take back to bare wood and reprime.

39 	Steel preparation

- Areas of defective primer, corrosion and loose scale: Take back to bare metal. Reprime as soon as possible.

- Defective paintwork: Remove to leave a firm edge and clean bright metal.

- Sound paintwork: Provide key for subsequent coats.

- Corrosion and loose scale: Take back to bare metal.

- Residual rust: Treat with a proprietary removal solution.

- Bare metal: Apply primer as soon as possible.

- Remaining areas: Degrease.

41 	Masonry and rendering preparation

- Loose and flaking material: Remove.

43 	Plaster preparation

- Nibs, trowel marks and plaster splashes: Scrape off.

- Overtrowelled 'polished' areas: Provide suitable key.

- Depressions around fixings: Fill with stopper/ filler.

45 	Previously painted window frames

- Paint encroaching beyond glass sight line: Remove.

- Loose and defective putty: Remove.

- Putty cavities and junctions between previously painted surfaces and glass: Clean thoroughly.

- Finishing

  - Patch prime, reputty, as necessary and allow to harden.

  - Seal and coat as soon as sufficiently hard.

50 	External pointing to existing frames

- Defective sealant pointing: Remove.

- Joint depth: Approximately half joint width; adjust with backing strip if necessary.

- Sealant

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Preparation and application: As section Z22.

52 	Sealing of internal movement joints

- General: To junctions of walls and ceilings with architraves, skirtings and other trims.

- Sealant: Water-borne acrylic.

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Preparation and application: As section Z22.

55 	Existing gutters

- Dirt and debris: Remove from inside of gutters.

- Defective joints: Clean and seal with suitable jointing material.

- Suspected hazardous materials: submit method statement.

61 	Coating generally

- Application: In accordance with BS 6150,

- Conditions: Maintain suitable temperature, humidity and air quality.

- Surfaces: Clean and dry at time of application.

- Thinning and intermixing: Not permitted unless recommended by manufacturer.

- Overpainting: Do not paint over intumescent strips or silicone mastics.

- Priming coats: Apply as soon as possible on same day as preparation is completed.

- Finish

  - Even, smooth and of uniform colour.

  - Free from brush marks, sags, runs and other defects.

  - Cut in neatly.

- Doors, opening windows and other moving parts: Ease before coating and between coats.

65 	Concealed joinery surfaces

- General: After priming, apply additional coatings to surfaces that will be concealed when component is fixed in place.

66 	Concealed metal surfaces

- General: Apply additional coatings to surfaces that will be concealed when component is fixed in place.

68 	Staining wood

- Primer: Apply, if recommended by stain manufacturer.

- Application: Apply in flowing coats and brush out excess stain to produce uniform appearance.

69 	Varnishing wood

- First coat: Thin with white spirit

  - Brush well in and lay off avoiding aeration.

- Subsequent coats: Provide light key along the grain between coats.

70 	External doors

- Bottom edges: Prime and coat before hanging.

75 	Bead glazing to coated wood

- Before glazing: Apply first two coats to rebates and beads.

80 	Linseed oil putty glazing

- Setting: Allow putty to set for seven days.

- Sealing

  - Within a further 14 days, seal with a solvent-borne primer.

  - Fully protect putty with coating system as soon as it is sufficiently hard.

  - Extend finishing coats on to glass up to sight line.

Ω End of Section

N13
Sanitary appliances and fittings

To be read with preliminaries/ general conditions.

10 	WC suites - w/o IPS panel backing Type A

- Pan: SanCeram Chartham close-coupled WC

  - Manufacturer: Bushboard Washroom Systems Ltd

    - Contact details

      - Address: Bushboard Washroom Systems Limited
Unit 1400, 1st Floor, Montagu Court
Kettering Venture Park
Kettering
Northamptonshire
United Kingdom
NN15 6XR

      - Telephone: +44 (0)1536 533620

      - Web: www.bushboard-washrooms.co.uk

      - Email: washrooms@bushboard-washrooms.co.uk

    - Product reference: Chartham Close Coupled WC

  - Form: Close-coupled WC pan and cistern.

  - Materials

    - Body: Vitreous china to BS 3402.

    - Finish and colour: Alpine White.

  - Sizes

    - Cistern capacity: 6/3 L dual flush.

    - Pan height: 405 mm.

  - Weight: 37.2 kg.

  - Toilet seat: Chartham soft close seat and cover, white.

  - Fixing: Floor fixed.

10 	WC suites - to IPS panels Type B

- Pan: SanCeram Chartham Back-to-Wall WC

  - Manufacturer: Bushboard Washroom Systems Ltd

    - Contact details

      - Address: Bushboard Washroom Systems Limited
Unit 1400, 1st Floor, Montagu Court
Kettering Venture Park
Kettering
Northamptonshire
United Kingdom
NN15 6XR

      - Telephone: +44 (0)1536 533620

      - Web: www.bushboard-washrooms.co.uk

      - Email: washrooms@bushboard-washrooms.co.uk

    - Product reference: Chartham Back to Wall WC

  - Form: Back-to-wall, box rim, washdown.

  - Pan height: 400 mm.

  - Materials

    - Body: Vitreous china to BS 3402.

    - Finish and colour: Alpine white.

  - Water supply, outlet and seat holes

    - Outlet: TSWC115: Convert to P trap.

    - Seat holes: Standard pattern.

  - Fixings: Floor fixing pack.

  - Weight: 22.7 kg.

  - Size:: 370 x 510 x 400 mm.

12 	Accessible WC equipment packages - LH Type A

- Manufacturer: Bushboard Washroom Systems Ltd

  - Contact details

    - Address: Bushboard Washroom Systems Limited
Unit 1400, 1st Floor, Montagu Court
Kettering Venture Park
Kettering
Northamptonshire
United Kingdom
NN15 6XR

    - Telephone: +44 (0)1536 533620

    - Web: www.bushboard-washrooms.co.uk

    - Email: washrooms@bushboard-washrooms.co.uk

  - Product reference: Doc M Pack with Close Coupled WC (Left Hand) (SCDMCCLG: Grey pack)

- Standards: In accordance with Approved Document M.

- Form: Complete accessible WC Doc M package and fittings.

- Arrangement: Close-coupled pack.

- Transfer handing: Left-hand.

- Material and colour

  - WC pans: Vitreous china, white.

  - WC seats: Plastics, grey.

  - Washbasins

    - Material: Vitreous china, white.

  - Handrails: Grey.

- Water supply fittings: TMV3 sequential mixer tap.

- Integral accessories: Toilet roll holder and back rest.

12 	Accessible WC equipment packages - RH Type B

- Manufacturer: Bushboard Washroom Systems Ltd

  - Contact details

    - Address: Bushboard Washroom Systems Limited
Unit 1400, 1st Floor, Montagu Court
Kettering Venture Park
Kettering
Northamptonshire
United Kingdom
NN15 6XR

    - Telephone: +44 (0)1536 533620

    - Web: www.bushboard-washrooms.co.uk

    - Email: washrooms@bushboard-washrooms.co.uk

  - Product reference: Doc M Pack with Close Coupled WC (Right Hand) (SCDMCCRG: Grey pack)

- Standards: In accordance with Approved Document M.

- Form: Complete accessible WC Doc M package and fittings.

- Arrangement: Close-coupled pack.

- Transfer handing: Right-hand.

- Material and colour

  - WC pans: Vitreous china, white.

  - WC seats: Plastics, grey.

  - Washbasins

    - Material: Vitreous china, white.

  - Handrails: Grey.

- Water supply fittings: TMV3 sequential mixer tap.

- Integral accessories: Toilet roll holder and back rest.

24 	Mixer taps Type A

- Manufacturer: Bushboard Washroom Systems Ltd

  - Contact details

    - Address: Bushboard Washroom Systems Limited
Unit 1400, 1st Floor, Montagu Court
Kettering Venture Park
Kettering
Northamptonshire
United Kingdom
NN15 6XR

    - Telephone: +44 (0)1536 533620

    - Web: www.bushboard-washrooms.co.uk

    - Email: washrooms@bushboard-washrooms.co.uk

  - Product reference: Chartham Mono Basin Mixer Tap

- Approvals: Water Regulations Advisory Scheme (WRAS)-approved.

- Form: Mono basin mixer tap.

- Materials

  - Body: Steel.

  - Finish and colour: Chrome-plated.

- Flow rate (maximum): 7.0 L/min at 7 bar.

- WorkingPressureRange: 0.2–5.0 bar.

30 	Wall-hung washbasins Type A

- Manufacturer: Bushboard Washroom Systems Ltd

  - Contact details

    - Address: Bushboard Washroom Systems Limited
Unit 1400, 1st Floor, Montagu Court
Kettering Venture Park
Kettering
Northamptonshire
United Kingdom
NN15 6XR

    - Telephone: +44 (0)1536 533620

    - Web: www.bushboard-washrooms.co.uk

    - Email: washrooms@bushboard-washrooms.co.uk

  - Product reference: Chartham Wall Hung 500 Washbasin

- Form: Wall-hung wash basin.

- Materials

  - Body: Vitreous china to BS 3402.

  - Finish and colour: Alpine white.

- Size: 500 x 195 x 380 mm.

- Water supply, overflow and waste holes

  - Water supply: Right hand tap hole.

  - Overflow: None.

  - Waste: Bottom waste outlet.

- Integral accessories: Basin fixings.

- Weight: 10 kg.

- Waste options: TSWC108

- Trap: A10R.

43 	Shower trays Type A

- Manufacturer: KALDEWEI UK Ltd

  - Contact details

    - Address: Kings Hall
St Ives Business Park
Parsons Green
St Ives
Cambridgeshire
PE27 4WY

    - Telephone: +44 (0)800 840 9770

    - Web: www.kaldewei.com

    - Email: sales-uk@kaldewei.com

  - Product reference: SUPERPLAN Low Profile Steel Enamel Shower Tray (SUPERPLAN 3851 - 900 x 1200 mm)

- Form: Rectangular.

- Materials

  - Body: Steel enamel.

  - Finish and colour: Alpine white.

- Size: 900 x 1200 mm.

- Waste hole: Ø90 mm.

- Integral accessories: Sealing kit.

- Net weight: 28 kg.

- Anti-slip finish: To DIN EN 16165, Category C (Invisable).

70 	Installation generally

- Standards: In accordance with BS 6465-1, -2 and -3.

- Assembly and fixing: Fix appliances securely to structure, without taking support from pipelines, level and plumb and so that surfaces designed to fall drain as intended.

- Fasteners: Non-ferrous or stainless steel.

- Jointing and bedding compounds: Recommended by manufacturers of appliances, accessories and pipes, to form watertight joints between appliances and backgrounds (except cisterns) and between appliances and discharge pipes.

- Supply and discharge pipework: Fix before appliances.

- Timing: Tiled backgrounds, other than splashbacks, complete before fixing appliances. Do not overstress tiles when fixing appliances.

- On completion: Components and accessories working correctly with no leaks.

- Labels and stickers: Remove.

75 	Installing cisterns

- Cistern operating components: Obtain from cistern manufacturer.

- Inlet and flushing valves: Match to pressure of water supply.

- Internal overflows: Into pan, to give visible warning of discharge.

- External overflows: Fix pipes to falls, and locate to give visible warning of discharge. Agree position.

76 	Installing taps

- Fixing: Secure against twisting.

- Seal with appliance: Watertight.

- Positioning: Hot tap to left of cold tap as viewed by user of appliance.

77 	Installing wastes and overflows

- Bedding: Waterproof jointing compound.

- Fixing: With resilient washer between appliance and backnut.

Ω End of Section

N15
Internal fire and safety signage systems

General - Not Used

System performance

205 	Design of internal signage systems

- Description: Internal Areas

- Design: Complete detailed design and submit before commencing work.

- Content: Signs including facing information, components, inserts, accessories and fixings necessary to complete the system.

- Proposals: Submit drawings, schedules, technical information, calculations and manufacturer's literature before commencing work.

210 	General requirements

- Signage and way guidance system design: Internal Areas

  - For fire escape and evacuation signage: In accordance with: BS 5499-4 or BS ISO 16069.

  - For way guidance systems: In accordance with BS ISO 16069.

  - For safety signs other than escape route signage: In accordance with: BS 5499-10.

220 	Sign design and format

- Description: Internal Areas

- Format: In accordance with BS EN ISO 7010

- Geometric shapes, colours and layout: In accordance with BS ISO 3864-1.

- Design principles for graphical symbols: In accordance with BS ISO 3864-3.

- Colorimetric and photometric properties of safety sign materials: In accordance with BS ISO 3864-4.

- Water safety: In accordance with BS EN ISO 7010.

Products

320 	Aluminium plate

- Description: FIRE DOOR SIGNAGE

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Finish: Manufacturer's standard

- Perimeters: Manufacturer's standard

- Supports/ fixings: Screw-fixed

Execution

610 	Fixing signs generally

- Installation:

- Secure, plumb and level.

- Fasteners and adhesives: As section Z20.

- Strength of fasteners: Sufficient to support live and dead loads.

- Fixings showing on surface of sign: Must not detract from the message being displayed.

Completion

910 	Documentation

- Submit

  - Manufacturer's maintenance instructions.

  - Guarantees, warranties, test certificates, record schedules and logbooks.

Ω End of Section

P12
Fire-stopping systems

General

10 	Fire-stopping to service penetrations

- Description: Through fire-resisting partitions

- Fire performance: As contract drawings.

- Penetration seal: Contractor's choice

  - Size: To match wall thickness

- Gap sealer: Intumescent mastic gap sealer, as clause 34.

- Capping sealant: Contractor's choice

  - Colour: To match substrate

- Verification

  - Submittals: Specification details, subcontractor certification.

  - Timing: 4 weeks prior to installation.

16 	Linear gap sealing

- Description: Between 1F Bedroom partitions

- Fire performance: As contract drawings

- Gap width or height (nominal): TBC

- Gap filler: Contractor's choice

- Capping sealant: Contractor's choice

  - Colour: Submit proposals

- Verification

  - Submittals: Specification details, subcontractor certification.

  - Timing: 4 weeks prior to installation.

Products

30 	Product certification

- Certification: For products specified generically, submit evidence of compliance with the specification

- Acceptable evidence: Accreditation by the United Kingdom Accreditation Service (UKAS) , British Board of Agrément (BBA)-certified

34 	Intumescent mastic

- Manufacturer: Contractor's choice

  - Product reference: Contractor's choice

40 	Mineral wool rigid batts

- Manufacturer: Contractor's choice

  - Product reference: Contractor's choice

- Standard: To BS EN 13162.

43 	Pipe collars

- Manufacturer: Contractor's choice

  - Product reference: Contractor's choice

- Type: Contractor's choice

47 	Sealants

- Manufacturer: Contractor's choice

  - Product reference: Contractor's choice

- Type: Contractor's choice

Execution

61 	Third-party-certified installers

- Certification: For the technical competency of the installer of the evidence of compliance with a third-party installation certification scheme

- Acceptable evidence: FIRAS installer certification, LPCB certification, UKAS Certificate of Accreditation

62 	Workmanship generally

- Gaps: Seal gaps between building elements and services, to provide fire resistance and resist the passage of smoke

- Adjacent surfaces: Prevent overrun of sealant or mortar on to finished surfaces

66 	Installing mineral wool batts

- Installing batts: Fit tight into void between the penetrating services and the surrounding construction to form a solid barrier.

- Face of batts: Flush with the surface of wall, floor or soffit

- Joints between batts: Butt joints; seal with fire-resisting sealant

- Gaps between services and barrier: Seal with fire-resisting sealant

67 	Applying intumescent putty

- Sequence: Install putty after services are permanently installed.

- Loose dust and combustible materials: Remove from the opening, along with any other debris.

- Putty cure: Do not disturb putty before final set has taken place.

68 	Fixing pipe collars

- Collar fixing: Contractor's choice

- Gap around collar: Seal with gap filler and sealant

- Length of wraps: Not applicable

73 	Applying sealants generally

- Application: As section Z22

Completion

91 	Cleaning

- Masking tapes: Remove

- Cleaning: Clean off splashes and droppings. Wipe down finishes

92 	Inspection

- Notice for inspection (minimum): Five working days

Ω End of Section

P21
Door/ window ironmongery

To be read with preliminaries/ general conditions.

3 	Quantities and locations

- Quantities and locations of ironmongery are in the door and ironmongery schedule .

- Fixing: As sections L10 and L20.

5 	Ironmongery from single proprietary range

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Principal material/ finish: Satin stainless steel, grade 1.4301 (304)

- Items unavailable within selected range: Submit proposals.

6 	Samples

- General: Before placing orders with suppliers submit labelled samples of the following: Door latches, backplates, mortice locks.

  - Conformity: Retain samples on-site for the duration of the Contract. Ensure conformity of ironmongery as delivered with labelled samples.

8 	Door hinges

- Description: Fire Door Hinges

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Type: As schedule

- Size: As schedule

- Material/ finish: Satin stainless steel, grade 1.4301 (304)

- Other requirements: None

12 	Overhead door closers

- Description: Fire Door Overhead Closers

- Standard: To BS EN 1154.

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Power size: Adjustable 2-6

- Casing finish: Colour as door furniture

- Operational adjustment

  - Variable power: Matched to size, weight and location of doors. Fully closing latched doors and holding unlatched doors closed.

  - Closing against smoke seals of fire doors: Positive. No gaps.

24 	Door locks

- Standard: To BS EN 12209.

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Type: As schedule

- Backset: As schedule

- Material/ finish: Stainless steel faceplate

- Keying: As schedule

28 	Door latches

- Description: To doors

- Standard: To BS EN 12209.

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Type: Vertical case mortice latch

- Backset: As schedule

- Material/ finish: Stainless steel faceplate

- Latch spring strength: Select to prevent unsprung lever handles drooping.

32 	Panic exit devices Type A

- Description: To D.22 and D.23 (Pole Drop doors) (to be installed at high level)

- Standard: To BS EN 1125.

- Manufacturer: ASSA ABLOY Opening Solutions UK & Ireland

  - Contact details

    - Address: ASSA ABLOY UK Ltd
School Street
Willenhall
West Midlands
WV13 3PW

    - Telephone: 0845 223 2124

    - Web: www.assaabloy.co.uk

    - Email: nbs@assaabloy.com

  - Product reference: ASSA ABLOY - Exidor 297 Push Pad

- Standard: EN 179:2008.

- Classification grades (minimum)

  - Category of use: To BS EN 1125, grade 3.

  - Durability: To BS EN 1125, grade 7.

  - Door mass: To BS EN 1125, grade 6.

  - Suitability for use on fire and smoke doors: To BS EN 1125, grade 1.

  - Safety: To BS EN 1125, grade 1.

  - Corrosion resistance: To BS EN 1125, grade 3.

  - Security: To BS EN 1125, grade 4.

  - Projection of bar: To BS EN 1125, grade 2.

  - Type of bar operation: To BS EN 1125, grade B.

  - Field of door application: To BS EN 1125, grade A.

- Material and finish: Powder coated.

- Colour: Silver.

- Execution: Fasteners for hardware (to be installed at high level).

36 	Privacy indicator bolts

- Description: To WC Doors

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Type: Rotary, internal thumbturn integral with lever handle

- Material/ finish: Satin stainless steel, grade 1.4401 (316)

- Emergency release facility: Required.

38 	Lever handles

- Description: Handles for Internal Doors

- Standard: To BS EN 1906.

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Style: Round pattern with return to door

- Material/ finish: Satin stainless steel, grade 1.4301 (304)

- Mounting: Round sprung rose

42 	Pull handles

- Description: To doors as per schedule

- Standard: To BS 8424.

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Shape: D handle

- Diameter: 19 mm

- Distance between centres: 225 mm

- Material/ finish: Satin stainless steel, grade 1.4301 (304)

- Mounting: Bolt through

44 	Push plates

- Description: To doors as per schedule

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Size: As schedule

- Material/ finish: Satin stainless steel, grade 1.4301 (304)

- Mounting: Face fix

46 	Kick plates

- Description: To all doors

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Size: As schedule

- Material/ finish: Satin stainless steel, grade 1.4301 (304)

- Mounting: Face fix

48 	Escutcheons

- Description: To doors with lever handles and thumbturn locks

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Material/ finish: Satin stainless steel, grade 1.4301 (304)

- Keyhole type: Euro profile cylinder

50 	Door stops

- Description: Wall-mounted door stops

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Type: Wall-mounted, face-fixed, SAA finish, 75mm projection

58 	Door mounted coat hooks

- Description: To Accessible WC's

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Type: Coat hook

- Material/ finish: Satin stainless steel, grade 1.4301 (304)

66 	Door mounted air transfer grilles

- Description: To WC doors as per schedule

- Manufacturer: Submit proposals

  - Product reference: Submit proposals

- Type: As schedule

- Size: As schedule

- Material/ finish: Satin stainless steel, grade 1.4301 (304)

Ω End of Section

P31
Holes, chases, covers and supports for services

Clauses

10 	Holes, recesses and chases in masonry

- Standard: NHBC Standards and to BS 7671.

- Position: To maintain integrity of strength, stability and sound resistance of construction.

  - Parallel chasing: Offset chases by at least the thickness of the wall they are cut into to ensure chases are not positioned back to back on the same wall

- Holes

  - Diameter (maximum): 300 mm2.

  - Diameter (minimum): Minimum needed to accommodate services

- Walls of hollow or cellular masonry units: Do not chase

- Walls of solid masonry units

  - Vertical chases: No deeper than one third of single leaf thickness, excluding finishes.

  - Horizontal or raking chases: No longer than 1 m and no deeper than one sixth of the single leaf thickness, excluding finishes.

- Cutting: Do not set back to back. Offset by a clear distance at least equal to the wall thickness.

- Performance: Maintain minimum EI 60 fire resistance to be achieved in accordance with EN 13051-2.

20 	Notches and holes in structural timber

- General: Avoid if possible.

- Sizes: Minimum needed to accommodate services.

- Position: Do not locate near knots or other defects.

- Notches and holes in same joist: Minimum 100 mm apart horizontally.

- Notches in joists

  - Position: Locate at top. Form by sawing down to a drilled hole.

  - Depth (maximum): 0.125 x joist depth.

  - Distance from supports: Between 0.07 and 0.25 x span.

- Holes in joists

  - Position: Locate on neutral axis.

  - Diameter (maximum): 0.25 x joist depth

  - Centres (minimum): 3 x diameter of largest hole

  - Distance from supports: Between 0.25 and 0.4 of span.

- Notches in roof rafters, struts and truss members: Not permitted.

- Holes in struts and columns: Locate on neutral axis.

  - Diameter (maximum): 0.25 x minimum width of member

  - Centres (minimum): 3 x diameter of largest hole

  - Distance from ends: Between 0.25 and 0.4 of span.

- Performance: Maintain minimum EI 60 fire resistance to be achieved in accordance with EN 13051-2.

30 	Pipe sleeves

- Material: To match pipeline.

- Sleeves: Extend through full thickness of wall or floor. Position accurately.

  - Clearance around service (maximum): 20 mm or diameter of service, whichever is the lesser.

- Performance: Bed solid.
Maintain minimum EI 60 fire resistance to be achieved in accordance with EN 13051-2.

40 	Sealing around services

- Description: As Section P12.

- Standard: To BS 6214.

- Service: As drawings

- Location: Pipe sleeves through walls and floors. Walls and floors

- Sealing material: Intumescent sealant

- Method: Completely fill gaps with sealant and finish neatly

- Requirements: Prevent the spread of fire

- Performance: Maintain minimum EI 60 fire resistance to be achieved in accordance with EN 13051-2.

- Verification: Photographic evidence.

  - Submittals: Photographic evidence.

  - Timing: Issue as work is completed. Issue all 2 weeks prior to handover.

Ω End of Section

Z10
Purpose-made joinery

To be read with preliminaries/ general conditions.

110 	Fabrication

- Standard: To BS 1186-2.

- Sections: Accurate in profile and length, and free from twist and bowing. Formed out of solid unless shown otherwise.

  - Machined surfaces: Smooth and free from tearing, wooliness, chip bruising and other machining defects.

- Joints: Tight and close fitting.

- Assembled components: Rigid. Free from distortion.

- Screws: Provide pilot holes.

  - Screws of 8 gauge (4 mm diameter) or more and screws into hardwood: Provide clearance holes.

  - Countersink screws: Heads sunk at least 2 mm below surfaces visible in completed work.

  - Adhesives: Compatible with wood preservatives applied and end uses of timber.

120 	Cross section dimensions of timber

- General: Dimensions on drawings are finished sizes.

- Maximum permitted deviations from finished sizes

  - Softwood sections: To BS EN 1313-1:-

    - Clause 6 for sawn sections.

  - Hardwood sections: To BS EN 1313-2:-

    - Clause 6 for sawn sections.

    - Clause NA.3 for further processed sections.

130 	Preservative treated wood

- Cutting and machining: Completed as far as possible before treatment.

- Extensively processed timber: Retreat timber sawn lengthways, thicknessed, planed, ploughed, etc.

- Surfaces exposed by minor cutting and/ or drilling: Treat as recommended by main treatment solution manufacturer.

140 	Moisture content

- Wood and wood-based products: Maintained within range specified for the component during manufacture and storage.

250 	Finishing

- Surfaces: Smooth, even and suitable to receive finishes.

  - Arrises: Eased unless shown otherwise on drawings.

- End grain in external components: Sealed with primer or sealer as section M60 and allowed to dry before assembly.

Ω End of Section

Z11
Purpose-made metalwork

Products

310 	Materials generally

- Grades of metals, section dimensions and properties: To appropriate British Standards. When not specified, select grades and sections appropriate for the purpose.

- Prefinished metal: May be used if methods of fabrication do not damage or alter appearance of finish, and finish is adequately protected.

- Fasteners: To appropriate British Standards and, unless specified otherwise, of same metal as component being fastened, with matching coating or finish.

Fabrication

515 	Fabrication generally

- Contact between dissimilar metals in components: Avoid.

- Finished components: Rigid and free from distortion, cracks, burrs and sharp arrises.

  - Moving parts: Free moving without binding.

- Corner junctions of identical sections: Mitre.

520 	Cold formed work

- Profiles: Accurate, with straight arrises.

527 	Welding

- Description: Generally

- Welding procedures

  - Method and standard: Metal arc welding to BS EN 1011-1 and -2.
TIG welding to BS EN 1011-3
TIG or MIG welding to BS EN 1011-4

  - Welding Procedure Specification (WPS): Not required

- Preparation

  - Joint preparation: Clean thoroughly.

  - Surfaces of materials that will be self-finished and visible in the completed work: protect from weld splatter.

- Jointing

  - Joints: Fully bond parent and filler metal throughout with no inclusions, holes, porosity or cracks.

  - Dissimilar metals: Filler metal grade to be approved by a qualified metallurgist

  - Strength requirements: Welds to achieve design loads.

  - Heat straightening: Obtain approval

  - Complex assemblies: Agree priority for welding members to minimize distortion caused by subsequent welds.

  - Tack welds: Use only for temporary attachment.

  - Jigs: Provide to support and restrain members during welding.

  - Filler plates: Obtain approval

  - Lap joints: Minimum 5 x metal thickness or 25 mm, whichever is greater.

  - Weld terminations: Clean and sound.

Finishing

710 	Finishing welded and brazed joints visible in complete work

- Standard: To BS EN ISO 8501-3.

  - Preparation grade: P1

- Butt joints: Smooth, and flush with adjacent surfaces.

- Fillet joints: Neat.

- Grinding: Grind smooth where indicated on drawings.

745 	Preparation for application of coatings

- General: Complete fabrication, and drill fixing holes before applying coatings.

- Paint, grease, flux, rust, burrs and sharp arrises: Remove.

780 	Galvanizing

- Standard: To BS EN ISO 1461.

- Preparation

  - Vent and drain holes: Provide in accordance with BS EN 14713-1 and -2. Seal after sections have been drained and cooled.

  - Components subjected to cold working stresses: Heat treat to relieve stresses before galvanizing.

  - Welding slag: Remove.

  - Component cleaning: To BS EN ISO 8501-3.

  - Grade: St 2½

Ω End of Section

Z12
Preservative/ flame-retardant treatment

To be read with preliminaries/ general conditions.

110 	Treatment application

- Timing: After cutting and machining timber, and before assembling components.

- Processor: WPA benchmark-accredited for the specified treated components

120 	Preservative treatment performance

- Standard: In accordance with Table 5 of the WPA Code of practice

130 	Preservative treatment solution strengths/ treatment cycles

- General: Select to achieve specified service life and to suit treatability of specified wood species

140 	Copper-organic preservative treatment

- Solution

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Colour: Contractor's choice

  - Application: High-pressure impregnation.

- Moisture content of wood

  - At time of treatment: As specified for the timber/ component at time of fixing.

  - After treatment: Timber to be surface dry before use.

150 	Water-based organic preservative treatment

- Solution

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Application: High-pressure impregnation.

- Moisture content of wood

  - At time of treatment: As specified for the timber/ component at time of fixing.

  - After treatment: Timber to be surface dry before use.

160 	Organic solvent preservative treatment

- Solution

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Application: Double-vacuum and low-pressure impregnation, or immersion.

- Moisture content of wood

  - At time of treatment: As specified for the timber/ component at time of fixing.

  - After treatment: Timber to be surface dry before use.

165 	Water-based microemulsion preservative treatment

- Solution

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Application: Double-vacuum and low-pressure impregnation.

- Moisture content of wood

  - At time of treatment: As specified for the timber/ component at time of fixing.

  - After treatment: Timber to be surface dry before use.

167 	Boron compound preservative treatment

- Solution

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Application: High-pressure impregnation

- Moisture content of wood

  - At time of treatment: As specified for the timber/ component at time of fixing.

  - After treatment: Timber to be surface dry before use.

210 	Flame-retardant treatment

- Standard: In accordance with the WPA publication Flame Retardant Treatments - An Overview and supporting guidance notes

- Solution type: INT 1 or INT 2

  - Manufacturer: Contractor's choice

    - Product reference: Contractor's choice

  - Application: Incorporated during manufacture or Surface-applied intumescent coating.

- Reaction to fire performance: To BS EN 13501-1, Class B

- Moisture content of wood

  - At time of treatment: As specified for the timber/ component at time of fixing

  - After treatmen: Timber to be re-dried slowly at temperatures not exceeding 60°C to minimize distortion and degradation

610 	Making good to preservative treatment on site

- Preservative solution: Compatible with off-site treatment.

- Application: In accordance with preservative manufacturer's recommendations.

620 	Making good to flame-retardant treatment on site

- Flame-retardant: Compatible with off-site treatment.

- Application: In accordance with flame-retardant manufacturer's recommendations.

Ω End of Section

Z20
Fixings and adhesives

Products

310 	Fasteners generally

- Materials: To have:

  - Bimetallic corrosion resistance appropriate to items being fixed.

  - Atmospheric corrosion resistance appropriate to fixing location.

- Appearance: Submit samples on request.

320 	Packings

- Materials: Non-compressible, corrosion proof.

- Area of packings: Sufficient to transfer loads.

340 	Masonry fixings

- Light duty: Plugs and screws.

- Heavy duty: Expansion anchors or chemical anchors.

350 	Plugs

- Type: Proprietary types to suit substrate, loads to be supported and conditions expected in use.

390 	Adhesives generally

- Standards

  - Hot-setting phenolic and aminoplastic: To BS 1203.

  - Thermosetting wood adhesives: To BS EN 12765.

  - Thermoplastic adhesives: To BS EN 204.

410 	Powder actuated fixing systems

- Types of fastener, accessories and consumables: As recommended by tool manufacturer.

Execution

610 	Fixing generally

- Integrity of supported components: Select types, sizes, quantities and spacings of fixings, fasteners and packings to retain supported components without distortion or loss of support.

- Components, substrates, fixings and fasteners of dissimilar metals: Isolate with washers/ sleeves to avoid bimetallic corrosion.

- Appearance: Fixings to be in straight lines at regular centres.

620 	Fixing through finishes

- Penetration of fasteners and plugs into substrate: To achieve a secure fixing.

630 	Fixing packings

- Function: To take up tolerances and prevent distortion of materials and components.

- Limits: Do not use packings beyond thicknesses recommended by fixings and fasteners manufacturer.

- Locations: Not within zones to be filled with sealant.

640 	Fixing cramps

- Cramp positions: Maximum 150 mm from each end of frame sections and at 600 mm maximum centres.

- Fasteners: Fix cramps to frames with screws of same material as cramps.

- Fixings in masonry work: Fully bed in mortar.

670 	Pelleted countersunk screw fixing

- Finished level of countersunk screw heads: Minimum 6 mm below timber surface.

- Pellets: Cut from matching timber, match grain and glue in to full depth of hole.

- Finished level of pellets: Flush with surface.

680 	Plugged countersunk screw fixing

- Finished level of countersunk screw heads: Minimum 6 mm below timber surface.

- Plugs: Glue in to full depth of hole.

- Finished level of plugs: Projecting above surface.

690 	Using powder actuated fixing systems

- Powder actuated fixing tools: To BS 4078-2 and Kitemark certified.

- Operatives: Trained and certified as competent by tool manufacturer.

700 	Applying adhesives

- Surfaces: Clean. Adjust regularity and texture to suit bonding and gap filling characteristics of adhesive.

  - Support and clamping during setting: Provide as necessary. Do not mark surfaces of or distort components being fixed.

- Finished adhesive joints: Fully bonded. Free of surplus adhesive.

Ω End of Section

Z21
Mortars

Cement gauged mortars

110 	Cement gauged mortar mixes

- Specification: Proportions and additional requirements for mortar materials are specified elsewhere.

120 	Sand for site made cement gauged masonry mortars

- Standard: To BS EN 13139.

- Grading: 0/2 (FP or MP).

  - Fines content where the proportion of sand in a mortar mix is specified as a range (e.g. 1:1: 5-6):

    - Lower proportion of sand: Use category 3 fines.

    - Higher proportion of sand: Use category 2 fines.

- Sand for facework mortar: Maintain consistent colour and texture. Obtain from one source.

131 	Ready-Mixed lime:sand for cement gauged masonry mortars

- Standard: To BS EN 998-2.

- Lime: Nonhydraulic to BS EN 459-1.

  - Type: CL 90S.

- Pigments for coloured mortars: To BS EN 12878.

135 	Site made lime:sand for cement gauged masonry mortars

- Permitted use: Where a special colour is not required and in lieu of factory made ready-mixed material.

- Lime: Nonhydraulic to BS EN 459-1.

  - Type: CL 90S.

- Mixing: Thoroughly mix lime with sand, in the dry state. Add water and mix again. Allow to stand, without drying out, for at least 16 hours before using.

160 	Cements for mortars

- Cement: To BS EN 197-1 and CE marked.

  - Types: Portland cement, CEM I.

- Portland limestone cement, CEM ll/A-L or CEM ll/A-LL.

- Portland slag cement, CEM II/B-S.

- Portland fly ash cement, CEM II/B-V.

  - Strength class: 32.5, 42.5 or 52.5.

- White cement: To BS EN 197-1 and CE marked.

  - Type: Portland cement, CEM I.

  - Strength class: 52.5.

- Sulfate resisting Portland cement

  - Types: To BS EN 197-1 Sulfate resisting Portland cement, CEM I/SR and CE marked.

- To BS EN 197-1 fly ash cement, CEM ll/B-V and CE marked.

  - Strength class: 32.5, 42.5 or 52.5.

- Masonry cement: To BS EN 413-1 and CE marked.

  - Class: MC 12.5.

180 	Admixtures for site made cement gauged mortars

- Air entraining (plasticizing) admixtures: To BS EN 934-3 and compatible with other mortar constituents.

- Other admixtures: Submit proposals.

- Prohibited admixtures: Calcium chloride, ethylene glygol and any admixture containing calcium chloride.

190 	Retarded ready to use cement gauged masonry mortars

- Standard: BS EN 998-2.

- Lime for cement:lime:sand mortars: Nonhydraulic to BS EN 459-1.

  - Type: CL 90S.

- Pigments for coloured mortars: To BS EN 12878.

- Time and temperature limitations: Use within limits prescribed by mortar manufacturer.

  - Retempering: Restore workability with water only within prescribed time limits.

210 	Making cement gauged mortars

- Batching: By volume. Use clean and accurate gauge boxes or buckets.

  - Mix proportions: Based on dry sand. Allow for bulking of damp sand.

- Mixing: Mix materials thoroughly to uniform consistency, free from lumps.

  - Mortars containing air entraining admixtures: Mix mechanically. Do not overmix.

- Working time (maximum): Two hours at normal temperatures.

- Contamination: Prevent intermixing with other materials.

Lime:sand mortars - Not Used

Ω End of Section

Z22
Sealants

Products

310 	Joints

- Manufacturer: Contractor's choice

  - Product reference: Contractor's choice

- Primer, backing strip, bond breaker: Types recommended by sealant manufacturer.

- Fire performance

  - Fire resistance: To BS EN 13501-2, EI 30 or better

  - Reaction to fire: To BS EN 13501-1, Class F or better

Execution

610 	Suitability of joints

- Presealing checks

  - Joint dimensions: Within limits specified for the sealant.

  - Substrate quality: Surfaces regular, undamaged and stable.

- Joints not fit to receive sealant: Submit proposals for rectification

620 	Preparing joints

- Surfaces to which sealant must adhere

  - Remove temporary coatings, tapes, loosely adhering material, dust, oil, grease, surface water and contaminants that may affect bond.

  - Clean using materials and methods recommended by sealant manufacturer.

- Vulnerable surfaces adjacent to joints: Mask to prevent staining or smearing with primer or sealant.

- Backing strip and/ or bond breaker installation: Insert into joint to correct depth, without stretching or twisting, leaving no gaps.

- Protection: Keep joints clean and protect from damage until sealant is applied.

630 	Applying sealants

- Substrate: Dry (unless recommended otherwise) and unaffected by frost, ice or snow.

- Environmental conditions: Do not dry or raise temperature of joints by heating.

- Sealant application: Fill joints completely and neatly, ensuring firm adhesion to substrates.

- Sealant profiles

  - Butt and lap joints: Slightly concave.

  - Fillet joints: Flat or slightly convex.

- Protection: Protect finished joints from contamination or damage until sealant has cured.

Ω End of Section

Specification created using NBS Chorus